## Slide 1: Section 10 Bandstructure in Real Materials (Si, Ge, GaAs)
Solid State Devices

## Slide 2: Section 10 Bandstructure in Real Materials (Si, Ge, GaAs)
Original
Problem
Periodic
Structure
E
U
Section 7 – Bandstructure in 1D Periodic Potentials
Section 8 – Brillouin Zone - Reciprocal Lattice
Section 9 – Constant Energy Surfaces & DOS
10.1 E(k) diagrams in specific crystal directions
10.2 Constant Energy Surfaces – Effective Mass Tensor
10.3 Density of States Effective Mass
Reference: Vol. 6, Ch. 3

## Slide 3: Analogy for E-k Diagram: 4D info through 2D Plots
Density (x,y,z)
4D information
Cut along (1, 1) …
r
r
1
1
A series of line-sections can
Represent the 4D info in 2D plots

## Slide 4: E-k along G-X Direction
Ge

## Slide 5: E-k along G-X Direction
Ge

## Slide 6: E-k along G-X Direction
Ge

## Slide 7: E-k Diagram – Dispersion for Ge, Si, GaAs
Minima may not be at zone center
(Ge: 8 L valleys, Si: 6 X valleys, and GaAs: G valleys)

## Slide 8: E-k Diagram – Dispersion for Ge, Si, GaAs
3 valence bands (light hole, heavy hole, split-off)
valence bands near k=0 is essentially E ~ k2
Minima may not be at zone center
(Ge: 8 L valleys, Si: 6 X valleys, and GaAs: G valleys)

## Slide 9: E-k diagram for GaAs
Direct bandgap material
Zone-edge gaps (L6-G8,
X6-G8) close to direct gap
Has important implications
For transport

## Slide 10: Arrangement of Atoms
Poly-crystalline
Thin Film
Transistors
Crystalline
Amorphous
Oxides

## Slide 11: Poly-crystalline material
Isotropic bandgap and increase in scattering

## Slide 12: Band-structure and Periodicity
Periodicity is sufficient, but not necessary for bandgap.
Many amorphous material show full isotropic bandgap
PRB, 4, 2508, 1971
Edagawa, PRL, 100,013901, 2008

## Slide 13: Section 10 Bandstructure in Real Materials (Si, Ge, GaAs)
10.1 E(k) diagrams in specific crystal directions
10.2 Constant Energy Surfaces – Effective Mass Tensor
10.3 Density of States Effective Mass
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 3
One Video Segment
status

## Slide 14: Section 10 Bandstructure in Real Materials (Si, Ge, GaAs)
10.1 E(k) diagrams in specific crystal directions
10.2 Constant Energy Surfaces – Effective Mass Tensor
10.3 Density of States Effective Mass
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 3
One Video Segment
status

## Slide 15: Section 10 Bandstructure in Real Materials (Si, Ge, GaAs)
Solid State Devices
10.2 Constant Energy Surfaces – Effective Mass Tensor

## Slide 16: Section 10 Bandstructure in Real Materials (Si, Ge, GaAs)
10.1 E(k) diagrams in specific crystal directions
10.2 Constant Energy Surfaces – Effective Mass Tensor
10.3 Density of States Effective Mass
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 3
One Video Segment
status

## Slide 17: Analogy for E-k Diagram
Density (x,y,z)
Contours of density ….

## Slide 18: Four valleys (8 halves) inside BZ for Germanium

## Slide 19: Constant-E surface for Conduction Band

## Slide 20: Constant-E surface for Conduction Band

## Slide 21: Constant-E surface for Conduction Band

## Slide 22: Constant E-surface and Effective Mass Tensor
Offdiagonal Elements=0
=> Force and movement aligned
1 heavy mass
2 light masses
Ge: 8 valleys
Si: 6 valleys

## Slide 23: Constant E-surface for Valence Band

## Slide 24: Constant E-surface for Valence Band
Si: A=4.29, B=0.68, C=4.87; Ge: A=13.38, B=8.48, C=13.15
3 bands:
HH – Heavy Hole
LH – Light Hole
SO – Split-off band
HH and LH are NOT
Isotropic => NOT spheres => strong spatial variations
Rotated substrate technology at TI
Robert C. Bowen
Enhanced PMOS

## Slide 25: Section 10 Bandstructure in Real Materials (Si, Ge, GaAs)
10.1 E(k) diagrams in specific crystal directions
10.2 Constant Energy Surfaces – Effective Mass Tensor
10.3 Density of States Effective Mass
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 3
One Video Segment
status

## Slide 26: Section 10 Bandstructure in Real Materials (Si, Ge, GaAs)
10.1 E(k) diagrams in specific crystal directions
10.2 Constant Energy Surfaces – Effective Mass Tensor
10.3 Density of States Effective Mass
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 3
One Video Segment
status

## Slide 27: Section 10 Bandstructure in Real Materials (Si, Ge, GaAs)
Solid State Devices
10.3 Density of States Effective Mass

## Slide 28: Section 10 Bandstructure in Real Materials (Si, Ge, GaAs)
10.1 E(k) diagrams in specific crystal directions
10.2 Constant Energy Surfaces – Effective Mass Tensor
10.3 Density of States Effective Mass
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 3
One Video Segment
status

## Slide 29: Density of States of GaAs: Conduction/Valence Bands

## Slide 30: Four valleys (8 halves) inside BZ for Germanium

## Slide 31: Ellipsoidal Bands and DOS Effective Mass
Transform into …
k1
k2
k3
E=const. ellipsoid
const. E
Nel is number of equivalent ellipsoids

## Slide 32: DOS Effective Mass for Conduction Band

## Slide 33: Section 10 Bandstructure in Real Materials (Si, Ge, GaAs)
10.1 E(k) diagrams in specific crystal directions
10.2 Constant Energy Surfaces – Effective Mass Tensor
10.3 Density of States Effective Mass
E-k diagrams emerge from the solution of Schrödinger’s Eq.
E-k diagrams at which energy an electron with a specific crystal momentum can reside.
E-k diagrams depend on the underlying crystal symmetry
Only a fraction of the available states are occupied. The number of available states change with energy.
DOS of g(E) describes the number of available states in a small energy window around energy E
DOS is an important and useful characteristic of a material
Video
Video
Video