## Slide 1: Section 11 Bandstructure Measurements
Solid State Devices

## Slide 2: Section 11 Bandstructure Measurements
Original
Problem
Periodic
Structure
E
U
Section 7 – Bandstructure in 1D Periodic Potentials
Section 8 – Brillouin Zone - Reciprocal Lattice
Section 9 – Constant Energy Surfaces & DOS
Section 10 – Bandstructure in Real Materials (Si, Ge, GaAs)
11.1 Bandgap measurements
11.2 Effective mass measurements
Reference: Vol. 6, Ch. 3

## Slide 3: Reminder: Momentum vs. DOS
k
E
E
DOS
Important things to remember:
Momentum k entered our thinking as a quantum number
Each quantum number is creating ONE state
Often “just” need the number of available states in an energy range => Density of States => appears to be solely determined by
  1) band edge,
  2) effective mass

## Slide 4: Measurement of Band Gap
k
E
1
2
3
4
Photons are only absorbed between
bands that have filled and empty states
E23
absorption

## Slide 5: Measurement of Energy Gap
k
hn
Iout
Iin
E23
Iout - Iin
E23+D
k
E
1
2
3
4

## Slide 6: Direct Bandgaps
k
E
1
2
3
4
Photons are only absorbed between
bands that have filled and empty states
E23
absorption
Particle-particle interaction –
Energy and momentum must be conserved
Photon momentum negligible compared to electron momentum
Electron transition is “vertical”
https://en.wikipedia.org/wiki/Direct_and_indirect_band_gaps
https://upload.wikimedia.org/wikipedia/commons/thumb/7/7a/Direct.svg/600px-Direct.svg.png

## Slide 7: Direct Bandgaps
k
E
1
2
3
4
Particle-particle interaction –
Energy and momentum must be conserved
Photon momentum negligible compared to electron momentum
Electron transition is “vertical”
https://en.wikipedia.org/wiki/Direct_and_indirect_band_gaps
https://upload.wikimedia.org/wikipedia/commons/thumb/7/7a/Direct.svg/600px-Direct.svg.png
https://en.wikipedia.org/wiki/File:Bulkbandstructure.gif
https://upload.wikimedia.org/wikipedia/en/b/ba/Indirect_Bandgap.svg
In Si and Ge the smallest bandgap is not at G
nanoHUB result on wikipedia

## Slide 8: Direct and Indirect Bandgaps
k
E
1
2
3
4
Particle-particle interaction –
Energy and momentum must be conserved
Photon momentum negligible compared to electron momentum
Electron transition is “vertical”
https://en.wikipedia.org/wiki/Direct_and_indirect_band_gaps
https://upload.wikimedia.org/wikipedia/commons/thumb/7/7a/Direct.svg/600px-Direct.svg.png
https://en.wikipedia.org/wiki/File:Bulkbandstructure.gif
https://upload.wikimedia.org/wikipedia/en/b/ba/Indirect_Bandgap.svg
In Si and Ge the smallest bandgap is not at G
nanoHUB result on wikipedia
Need a “phonon” to compensate momentum conservation
3-particles - less efficient

## Slide 9: Temperature-dependent Band Gap
k
E
1
2
3
4

## Slide 10: Section 11 Bandstructure Measurements
Section 7 – Bandstructure in 1D Periodic Potentials
Section 8 – Brillouin Zone - Reciprocal Lattice
Section 9 – Constant Energy Surfaces & DOS
Section 10 – Bandstructure in Real Materials (Si, Ge, GaAs)
Bandstructure Measurements test and validate the theories
11.1 Bandgap measurements
11.2 Effective mass measurements
Reference: Vol. 6, Ch. 3
Video Segment
Video Segment
status

## Slide 11: Section 11 Bandstructure Measurements
Section 7 – Bandstructure in 1D Periodic Potentials
Section 8 – Brillouin Zone - Reciprocal Lattice
Section 9 – Constant Energy Surfaces & DOS
Section 10 – Bandstructure in Real Materials (Si, Ge, GaAs)
Bandstructure Measurements test and validate the theories
11.1 Bandgap measurements
11.2 Effective mass measurements
Reference: Vol. 6, Ch. 3
Video Segment
Video Segment
status

## Slide 12: Section 11 Bandstructure Measurements
Solid State Devices
11.2 Effective mass measurements

## Slide 13: Section 11 Bandstructure Measurements
Section 7 – Bandstructure in 1D Periodic Potentials
Section 8 – Brillouin Zone - Reciprocal Lattice
Section 9 – Constant Energy Surfaces & DOS
Section 10 – Bandstructure in Real Materials (Si, Ge, GaAs)
Bandstructure Measurements test and validate the theories
11.1 Bandgap measurements
Reference: Vol. 6, Ch. 3
Video Segment
Video Segment
status
11.2 Effective mass measurements

## Slide 14: 11.2 Effective mass measurements
Important things to remember:
Full bands do not conduct – electrons have no space to go
Empty bands to not conduct – there are no electrons to go around
Question:
We are interested in the top-most valence band holes and the bottom-most electron states
We want to figure out the slope of the bands
How can we probe just one particular species of electrons/holes?
We do not want to transfer them from one band to the next!
=> can we rotate the electrons around in a single band?
k
E
3
2
1

## Slide 15: Motion in Real Space and Phase Space
(kx,0)
(0,-ky)
(0,ky)
(-kx,0)
kx
Energy=constant.
kx
ky
kz
ky
Liquid He temperature …
x
y
Notes: df_s/dp_x=0 because f=exp(-p^2) df_s/dp=p*f_s sum p*f_s = 0

## Slide 16: Derive the Cyclotron Formula
B
For an particle in (x-y) plane with B-field in z-direction,
the Lorentz force is …

## Slide 17: Measurement of Effective Mass
n0=24 GHz
(fixed)
Iout
Iin
Measurement “easy” for spherical surfaces
Iin - Iout
B
Bcon
kx
ky
kz
Bval
kx
ky
kz
B field variable …

## Slide 18: Effective mass in Ge
4 symmetry angles between B field and the ellipsoids …
B
(in Si, there would 6 equivalent valleys, 3 specific directions)

## Slide 19: Cyclotron Formula for Multiple Valleys
B
Show that
The Lorentz force on electrons in a B-field
In other words,
Experiment looks at three q, and measures three mc
From this expression you derive mt, and ml
B0
ky
kx
kz

## Slide 20: Continued …
Let (B) make an angle (q) with longitudinal axis of the ellipsoid (ellipsoids oriented along kz)
B0
ky
kx
kz

## Slide 21: Continued …
Differentiate (vy) and use other equations to find …
Let (B) make an angle (q) with longitudinal axis of the ellipsoid (ellipsoids oriented along kz)
so that …
B0
ky
kx
kz

## Slide 22: Measurement of Effective Mass
Three peaks B1, B2, B3
Three masses mc1,mc2,mc3
Three unique angles: 7, 65, 73
Known q and mc allows calculation of mt and ml.
[110]
Magnetic Field
Picks 3 symmetry angles
B=[0.61, 0.61, 0.5]

## Slide 23: Valence Band Effective Mass
Which peaks relate to valence band?
Why are there two valence band peaks?

## Slide 24: Section 11 Bandstructure Measurements
Bandstructure Measurements test and validate the theories
11.1 Bandgap measurements
11.2 Effective mass measurements
Section 7 – Bandstructure in 1D Periodic Potentials
Section 8 – Brillouin Zone - Reciprocal Lattice
Section 9 – Constant Energy Surfaces & DOS
Section 10 – Bandstructure in Real Materials (Si, Ge, GaAs)
Reference: Vol. 6, Ch. 3
Video Segment
Video Segment
status