## Slide 1: Section 12 Occupation of States
Solid State Devices

## Slide 2: Section 12 Occupation of States
V
I
I = G x V
density
velocity
charge
area
= q x n x v x A
Number of carriers
available for conduction
Number of atoms/volume
from crystal structure
Number of electrons/atoms
Carrier number = Number of states x filling factor
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory

## Slide 3: Section 12 Occupation of States
V
I
I = G x V
density
velocity
charge
area
= q x n x v x A
Number of carriers
available for conduction
Number of atoms/volume
from crystal structure
Number of electrons/atoms
Carrier number = Number of states x filling factor
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Quantum Mechanics Mechanics
Concepts of density of states and masses

## Slide 4: Section 12 Occupation of States
V
I
I = G x V
density
velocity
charge
area
= q x n x v x A
Number of carriers
available for conduction
Number of atoms/volume
from crystal structure
Number of electrons/atoms
Carrier number = Number of states x filling factor
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Quantum Mechanics Mechanics
Concepts of density of states and masses

## Slide 5: Section 12 Occupation of States
V
I
I = G x V
density
velocity
charge
area
= q x n x v x A
Number of carriers
available for conduction
Number of atoms/volume
from crystal structure
Number of electrons/atoms
Carrier number = Number of states x filling factor
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses

## Slide 6: Section 12 Occupation of States
V
Transport with scattering, non-equilibrium Statistical Mechanics
Drift-diffusion equation with recombination-generation
I
Understanding transport in concrete devices
Diodes, BJT/HBT, MOS
I = G x V
density
velocity
charge
area
= q x n x v x A
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
Carrier number = Number of states x filling factor

## Slide 7: Section 12 Occupation of States
V
I
I = G x V
density
velocity
charge
area
= q x n x v x A
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
12.1 Rules of filling electronic states
12.2 Three Derivations of Fermi-Dirac Statistics
12.3 Intrinsic carrier concentration
Carrier number = Number of states x filling factor

## Slide 8: E-k diagram and Electronic States
g(E)
E
E1
E2
E3
Density of States

## Slide 9: Rules for filling up the States
Pauli Principle: Only one electron per state
Total number of electrons is conserved
Total energy of the system is conserved
E2
E3
E1

## Slide 10: Section 12 Occupation of States
12.1 Rules of filling electronic states
  Pauli exclusion
  Total particle conservation
  Total energy conservation
12.2 Derivation of Fermi-Dirac Statistics: three techniques
  Microcanonical ensemble - statistics
  Detailed Balance – thermal equilibrium & Pauli exclusion
  Partition Function – statistical mechanics
12.3 Intrinsic carrier concentration
  Fermi Integral
  Law of mass action
One Video Segment
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 4
Carrier number = Number of states x filling factor
status
E1
E2
E3

## Slide 11: Section 12 Occupation of States
12.1 Rules of filling electronic states
  Pauli exclusion
  Total particle conservation
  Total energy conservation
12.2 Derivation of Fermi-Dirac Statistics: three techniques
  Microcanonical ensemble - statistics
  Detailed Balance – thermal equilibrium & Pauli exclusion
  Partition Function – statistical mechanics
12.3 Intrinsic carrier concentration
  Fermi Integral
  Law of mass action
One Video Segment
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 4
Carrier number = Number of states x filling factor
status
E1
E2
E3

## Slide 12: Section 12 Occupation of States
Solid State Devices
12.2 Derivation of Fermi-Dirac Statistics

## Slide 13: Section 12 Occupation of States
12.1 Rules of filling electronic states
  Pauli exclusion
  Total particle conservation
  Total energy conservation
12.2 Derivation of Fermi-Dirac Statistics: three techniques
  Microcanonical ensemble - statistics
  Detailed Balance – thermal equilibrium & Pauli exclusion
  Partition Function – statistical mechanics
12.3 Intrinsic carrier concentration
  Fermi Integral
  Law of mass action
One Video Segment
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 4
Carrier number = Number of states x filling factor
status
E1
E2
E3

## Slide 14: Ensemble of 3 Energy Levels
E=0
E=2
E=4
ET=12
Particle conservation
Energy conservation
NT=5

## Slide 15: Occupation Statistics
E=0
E=2
E=4
W (E)
2,0,3 1,2,2 0,4,1
Choose the most
probable configuration.

## Slide 16: Occupation Statistics
E=0
E=2
E=4
Side note:
So far everything shown here is EXACT!
No approximations on the occupation probability! => direct application to nano-scale electronics!
Coulomb blockage Single electronics
W (E)
2,0,3 1,2,2 0,4,1

## Slide 17: Occupation Statistics
E=0
E=2
E=4
Side note:
So far everything shown here is EXACT!
No approximations on the occupation probability! => direct application to nano-scale electronics!
Coulomb blockage Single electronics
W (E)
2,0,3 1,2,2 0,4,1

## Slide 18: Occupation Statistics
E=0
E=2
E=4
Side note:
So far everything shown here is EXACT!
No approximations on the occupation probability! => direct application to nano-scale electronics!
Coulomb blockage Single electronics
W (E)
2,0,3 1,2,2 0,4,1

## Slide 19: Occupation Statistics
E=0
E=2
E=4
Side note:
So far everything shown here is EXACT!
No approximations on the occupation probability! => direct application to nano-scale electronics!
Coulomb blockage Single electronics
W (E)
2,0,3 1,2,2 0,4,1

## Slide 20: Occupation Statistics
E=0
E=2
E=4
Side note:
So far everything shown here is EXACT!
No approximations on the occupation probability! => direct application to nano-scale electronics!
Coulomb blockage Single electronics
W (E)
2,0,3 1,2,2 0,4,1

## Slide 21: Occupation Statistics
E=0
E=2
E=4
W (E)
2,0,3 1,2,2 0,4,1
f(E)
E
Side note:
So far everything shown here is EXACT!
No approximations on the occupation probability! => direct application to nano-scale electronics!
Coulomb blockage Single electronics

## Slide 22: Occupation Statistics
E=0
E=2
E=4
W (E)
2,0,3 1,2,2 0,4,1
f(E)
E
For large numbers of states, what is the most probably configuration?
configurations
Coulomb blockage Single electronics

## Slide 23: Occupation Statistics
Recall.
Si
Ni
Stirling approx.
configurations
For large numbers of states, what is the most probably configuration?
W (E)
2,0,3 1,2,2 0,4,1
Choose the most
probable
configuration.

## Slide 24: Optimization with Lagrange-Multiplier
For large numbers of states, what is the most probably configuration?
lnW
configurations
Lagrange multipliers at https://en.wikipedia.org/wiki/Lagrange_multiplier
Particle conservation
Energy conservation
Optimization with constraints!
Choose the most
probable
configuration.

## Slide 25: Final steps …
f(E)
E
fmax(E)=1
EF

## Slide 26: Section 12 Occupation of States
12.1 Rules of filling electronic states
  Pauli exclusion
  Total particle conservation
  Total energy conservation
12.2 Derivation of Fermi-Dirac Statistics: three techniques
  Microcanonical ensemble - statistics
  Detailed Balance – thermal equilibrium & Pauli exclusion
  Partition Function – statistical mechanics
12.3 Intrinsic carrier concentration
  Fermi Integral
  Law of mass action
One Video Segment
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 4
Carrier number = Number of states x filling factor
status

## Slide 27: Derivation by Detailed Balance
E=0
E=2
E=4
Pauli Exclusion
Detailed Balance in Equilibrium
full
empty
empty
full
full
empty
empty
full

## Slide 28: Derivation by Detailed Balance
Pauli Principle, energy, and number conservation all satisfied
Only solution is ….
E=0
E=2
E=4
Energy conversation
Pauli Exclusion
Detailed Balance in Equilibrium
A Note on the Use of the Principle of Detailed Balance in Obtaining the Fermi-Dirac Distribution Function, John E. Walsh: American Journal of Physics38, 392 (1970); doi: 10.1119/1.1976344

## Slide 29: Section 12 Occupation of States
12.1 Rules of filling electronic states
  Pauli exclusion
  Total particle conservation
  Total energy conservation
12.2 Derivation of Fermi-Dirac Statistics: three techniques
  Microcanonical ensemble - statistics
  Detailed Balance – thermal equilibrium & Pauli exclusion
  Partition Function – statistical mechanics
12.3 Intrinsic carrier concentration
  Fermi Integral
  Law of mass action
One Video Segment
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 4
Carrier number = Number of states x filling factor
status

## Slide 30: Derivation by Partition Function
Ei
E=0
E=2
E=4

## Slide 31: Derivation by Partition Function
Probability that state is filled ….
1
f(E)
EF
1/2
E
1
f(E)
EF
1/2
E
1

## Slide 32: Derivation by Partition Function
Probability that state is filled ….
1
f(E)
EF
1/2
E
1
f(E)
EF
1/2
E
1
Partition Function or Statistical Mechanics Approach also holds for single electronics!

## Slide 33: Temperature Dependence
1
f(E)
EF
1/2
E
https://commons.wikimedia.org/wiki/File:Fermi.gif another nanoHUB animation on Wikipedia
https://nanohub.org/tools/fermi
Hot electrons reach higher energy states
Cold electrons are “frozen” to lowest possible states

## Slide 34: Few comments on Fermi-Dirac Statistics
Applies to all spin-1/2 particles
Typically, information about spin is not explicit; multiply DOS by 2.
May be more complicated for magnetic semiconductors, Topological insulators, quantum computing, coulomb blockade etc
Coulomb-interaction among particles is neglected,
Therefore it applies to extended solids, not to small molecules
Lx

## Slide 35: Section 12 Occupation of States
12.1 Rules of filling electronic states
  Pauli exclusion
  Total particle conservation
  Total energy conservation
12.2 Derivation of Fermi-Dirac Statistics: three techniques
  Microcanonical ensemble - statistics
  Detailed Balance – thermal equilibrium & Pauli exclusion
  Partition Function – statistical mechanics
12.3 Intrinsic carrier concentration
  Fermi Integral
  Law of mass action
One Video Segment
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 4
Carrier number = Number of states x filling factor
In 1926, Fowler studied collapse of a star to white dwarf by F-D statistics, before Sommerfeld used the F-D statistics to develop a theory of electrons in metals in 1927. Wikipedia has a nice article on this topic.
status

## Slide 36: Section 12 Occupation of States
12.1 Rules of filling electronic states
  Pauli exclusion
  Total particle conservation
  Total energy conservation
12.2 Derivation of Fermi-Dirac Statistics: three techniques
  Microcanonical ensemble - statistics
  Detailed Balance – thermal equilibrium & Pauli exclusion
  Partition Function – statistical mechanics
12.3 Intrinsic carrier concentration
  Fermi Integral
  Law of mass action
One Video Segment
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 4
Carrier number = Number of states x filling factor
In 1926, Fowler studied collapse of a star to white dwarf by F-D statistics, before Sommerfeld used the F-D statistics to develop a theory of electrons in metals in 1927. Wikipedia has a nice article on this topic.
status

## Slide 37: Section 12 Occupation of States
Solid State Devices
12.3 Intrinsic carrier concentration

## Slide 38: Section 12 Occupation of States
12.1 Rules of filling electronic states
  Pauli exclusion
  Total particle conservation
  Total energy conservation
12.2 Derivation of Fermi-Dirac Statistics: three techniques
  Microcanonical ensemble - statistics
  Detailed Balance – thermal equilibrium & Pauli exclusion
  Partition Function – statistical mechanics
12.3 Intrinsic carrier concentration
  Fermi Integral
  Law of mass action
One Video Segment
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 4
Carrier number = Number of states x filling factor
status

## Slide 39: Carrier Distribution
DOS
F-D
concentration
1

## Slide 40: Electron Concentration in 3D solids
Assume wide bands
Include spin factor of 2

## Slide 41: Fermi Integral is Painful to Evaluate (not analytic – lookup tables or expensive numerical)
Boltzmann Statistics!
For non-degenerate systems

## Slide 42: Carrier Distribution => Effective Density of States
DOS
F-D
1
Charge Distribution
Delta Function Charge
No energy Distribution!
As if all states are at a single level EC

## Slide 43: Law of Mass-Action
Product is independent of the Fermi level!
Very useful balance equation! Will use it often

## Slide 44: Fermi-Level for Intrinsic Semiconductors
Notes: Need to restart on the quilibrium distribution!

## Slide 45: Section 12 Occupation of States
12.1 Rules of filling electronic states
  Pauli exclusion
  Total particle conservation
  Total energy conservation
12.2 Derivation of Fermi-Dirac Statistics: three techniques
  Microcanonical ensemble - statistics
  Detailed Balance – thermal equilibrium & Pauli exclusion
  Partition Function – statistical mechanics
12.3 Intrinsic carrier concentration
  Fermi Integral
  Law of mass action
One Video Segment
One Video Segment
One Video Segment
Reference: Vol. 6, Ch. 4
Carrier number = Number of states x filling factor
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
What’s Next?

## Slide 46: Section 12 Occupation of States
V
Transport with scattering, non-equilibrium Statistical Mechanics
Drift-diffusion equation with recombination-generation
I
Understanding transport in concrete devices
Diodes, BJT/HBT, MOS
I = G x V
density
velocity
charge
area
= q x n x v x A
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses