## Slide 1: Section 14 Doping
Solid State Devices

## Slide 2: Section 14 Doping
Transport with scattering, non-equilibrium Stat. Mech.
Drift-diffusion equation with recombination-generation
Understanding transport in concrete devices
Diodes, BJT/HBT, MOS
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
I = G x V
density
velocity
charge
area
= q x n x v x A
Semiconductor
  Ge: Eg=0.8eV ni~1013/cm3 0.1 in a billion
  Si: Eg=1.1eV ni~1010/cm3 0.1 in a trillion
  GaAs: Eg=1.42eV ni~106/cm3 1 in 1017
  Very weakly conducting
  Fermi level about midgap – no DOS
Not Enough Electrons available
Metal:
  Conducts electrons even at very low temperatures
  Fermi Level crosses multiple bands => large density of states at Fermi level

## Slide 3: Section 14 Doping
Transport with scattering, non-equilibrium Stat. Mech.
Drift-diffusion equation with recombination-generation
Understanding transport in concrete devices
Diodes, BJT/HBT, MOS
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
I = G x V
density
velocity
charge
area
= q x n x v x A
Semiconductor
  Ge: Eg=0.8eV ni~1013/cm3 0.1 in a billion
  Si: Eg=1.1eV ni~1010/cm3 0.1 in a trillion
  GaAs: Eg=1.42eV ni~106/cm3 1 in 1017
  Very weakly conducting
  Fermi level about midgap – no DOS
Metal:
  Conducts electrons even at very low temperatures
  Fermi Level crosses multiple bands => large density of states at Fermi level
Not Enough Electrons available
semiconductor

## Slide 4: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
Semiconductor
  Ge: Eg=0.8eV ni~1013/cm3 0.1 in a billion
  Si: Eg=1.1eV ni~1010/cm3 0.1 in a trillion
  GaAs: Eg=1.42eV ni~106/cm3 1 in 1017
  Very weakly conducting
  Fermi level about midgap – no DOS
Metal:
  Conducts electrons even at very low temperatures
  Fermi Level crosses multiple bands => large density of states at Fermi level
semiconductor
metal
Not Enough Electrons available
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Transport with scattering, non-equilibrium Stat. Mech.
Drift-diffusion equation with recombination-generation

## Slide 5: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
Semiconductor
  Ge: Eg=0.8eV ni~1013/cm3 0.1 in a billion
  Si: Eg=1.1eV ni~1010/cm3 0.1 in a trillion
  GaAs: Eg=1.42eV ni~106/cm3 1 in 1017
  Very weakly conducting
  Fermi level about midgap – no DOS
Metal:
  Conducts electrons even at very low temperatures
  Fermi Level crosses multiple bands => large density of states at Fermi level
semiconductor
metal
Insulator
  “Not” conducting – Fermi level midgap
  SiO2, Eg= 9eV, ni~10-68/cm3
    The whole earth has about 1050 atoms! If you made the whole world out of glass, there would be not one electron conductive at room temperature!
Not Enough Electrons available
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Transport with scattering, non-equilibrium Stat. Mech.
Drift-diffusion equation with recombination-generation

## Slide 6: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
Semiconductor
  Ge: Eg=0.8eV ni~1013/cm3 0.1 in a billion
  Si: Eg=1.1eV ni~1010/cm3 0.1 in a trillion
  GaAs: Eg=1.42eV ni~106/cm3 1 in 1017
  Very weakly conducting
  Fermi level about midgap – no DOS
Metal:
  Conducts electrons even at very low temperatures
  Fermi Level crosses multiple bands => large density of states at Fermi level
semiconductor
Not Enough Electrons available
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
Materials, composition, crystals
Tabulated for “known” bulk materials
Transport with scattering, non-equilibrium Stat. Mech.

## Slide 7: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
https://commons.wikimedia.org/wiki/File:Band_filling_diagram.svg
semiconductor
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
14.1 Basic concepts of donors and acceptors
14.2 Statistics of donor and acceptor levels
14.3 Temperature dependence of carrier concentration
14.4 Multiple doping, co-doping, and heavy-doping
Video
Video
Video
Video
Materials, composition, crystals
Tabulated for “known” bulk materials
Transport with scattering, non-equilibrium Stat. Mech.

## Slide 8: Simplified Planar View of Atoms

## Slide 9: Donor Atoms
Even with donors, material
is charge neutral

## Slide 10: Donor Atoms in H2-analogy
=
+
r0
=
r0

## Slide 11: Donor Atoms in Real and Energy Space
ET=E1
~10s meV
1/b~kBT~25meV at T=300K
r0

## Slide 12: Assumption of Large Radius …
a~0.5nm=5A => hundreds of Si atoms
r0
ET=E1
~10s meV
1/b~kBT~25meV at T=300K

## Slide 13: Single Impurity / Donor in a modern FinFET
a~0.5nm=5A => hundreds of Si atoms
r0
ET=E1
~10s meV
1/b~kBT~25meV at T=300K

## Slide 14: Single Impurity / Donor in a modern FinFET
a~0.5nm=5A => hundreds of Si atoms
r0
ET=E1

## Slide 15: Single Impurity / Donor in a modern FinFET
r0
a~0.5nm=5A => hundreds of Si atoms
ET=E1

## Slide 16: Measurement of Donor Wavefunctions
Usman, M., Bocquel, J., Salfi, J. et al. Spatial metrology of dopants in silicon with exact lattice site precision. Nature Nanotech 11, 763–768 (2016). https://doi.org/10.1038/nnano.2016.83
r0
a~0.5nm=5A => hundreds of Si atoms
ET=E1

## Slide 17: Measurement of Donor Wavefunctions
Usman, M., Bocquel, J., Salfi, J. et al. Spatial metrology of dopants in silicon with exact lattice site precision. Nature Nanotech 11, 763–768 (2016). https://doi.org/10.1038/nnano.2016.83
r0
a~0.5nm=5A => hundreds of Si atoms
ET=E1

## Slide 18: Measurement of Donor Wavefunctions
Usman, M., Bocquel, J., Salfi, J. et al. Spatial metrology of dopants in silicon with exact lattice site precision. Nature Nanotech 11, 763–768 (2016). https://doi.org/10.1038/nnano.2016.83
a~0.5nm=5A => hundreds of Si atoms
ET=E1
r0

## Slide 19: Characteristics of Donor Atoms
The number of donor atoms is much smaller compared to host atoms. Therefore, the electrons from one donor atom can go to the other donor atoms only via the conduction /valence bands of the host crystal.
Just like a Hydrogen atom, it is possible to have multiple localized level for a given atom (see the blue levels).
Good donors live close to the conduction band, so that they can offer electrons easily. However, if they are below the midgap, the donor levels are marked with (D) to differentiate them from acceptor atoms (which live close to the valence band).
ET=E1
r0
(D)

## Slide 20: Acceptor Atoms
Even with acceptor, material
is charge neutral
r0

## Slide 21: Characteristics of Acceptor Atoms
A
ET
r0

## Slide 22: Amphoteric Dopants
acceptor-type
Donor-type
r0

## Slide 23: Table of Donors and Acceptors
r0

## Slide 24: Conclusion
Intrinsic carrier concentration is so small that semiconductor must be doped to make it useful.
A doping atom behaves like a H-atom, except that the dielectric constant and effective masses are given by by those of the host atom.
r0

## Slide 25: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
14.1 Basic concepts of donors and acceptors
14.2 Statistics of donor and acceptor levels
14.3 Temperature dependence of carrier concentration
14.4 Multiple doping, co-doping, and heavy-doping
Video
Video
r0
=
Video
Video
Not Enough Electrons available
A doping atom behaves like a H-atom, except that the dielectric constant and effective masses are given by by those of the host atom.

## Slide 26: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
14.1 Basic concepts of donors and acceptors
14.2 Statistics of donor and acceptor levels
14.3 Temperature dependence of carrier concentration
14.4 Multiple doping, co-doping, and heavy-doping
Video
Video
r0
=
Video
Video
Not Enough Electrons available
A doping atom behaves like a H-atom, except that the dielectric constant and effective masses are given by by those of the host atom.

## Slide 27: Section 14 Doping
Solid State Devices
14.2 Statistics of donor and acceptor levels

## Slide 28: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
14.1 Basic concepts of donors and acceptors
14.2 Statistics of donor and acceptor levels
14.3 Temperature dependence of carrier concentration
14.4 Multiple doping, co-doping, and heavy-doping
Video
Video
r0
=
Video
Video
Not Enough Electrons available
A doping atom behaves like a H-atom, except that the dielectric constant and effective masses are given by by those of the host atom.

## Slide 29: Localized vs. Band Electrons
E1  2p/Lx
E2  4p/Lx
E3  6p/Lx
E4  8p/Lx
E5  10p/Lx
E6  12p/Lx
E1’  2p/(Lx/2)
E2’  4p/(Lx/2)
E3’  6p/(Lx/2)
Lx
Lx/2
Lx/2
Two electrons (even with
opposite spin) can not
be at the same position
and same energy because
of electrostatic repulsion
Band electrons (with
opposite spin) need not
be at the same position,
so they can share occupy
same energy level.
When we divide space by a factor of 2, the number of states (e.g. 6 here) does not change.

## Slide 30: Looking ahead: Carrier-Density w/Doping
A bulk material must be charge neutral over all …
Further if the material is spatially homogenous
Let us see how the formula comes about …

## Slide 31: Characteristics of Donor Atoms
(D)
r0
ET

## Slide 32: Localized vs. Delocalized States
2N states/per-band (with spin)
2N-2 states/per-band (with spin)
r0

## Slide 33: Statistics of Donor Levels

## Slide 34: Statistics of Donor Levels
1/1 x x x
Coulomb interaction
forbids this configuration

## Slide 35: Statistics of Donor Levels
Probability that the donor
is empty (charged)
Probability that the donor
is filled with at least
one electron (neutral)
Note the extra factor ….

## Slide 36: Acceptor Atoms
State [1] …. Hole present … N-1 charges
State [0] … Hole filled …. N charges

## Slide 37: Statistics of Acceptor Levels in Si and Ge
1. Each atom contributes 2 states (up & down spin)
  to a band, therefore a band has 2N states.
2. Every time a host atom is replaced by a impurity atom, 2 states are disappear per a band and
  appear as localized states (sort of).
3. Therefore an acceptor atom close to hh and lh bands removes four states from those bands.
4. Because of Coulomb interaction only 1 hole can seat in these 4 states: the states are
  0000, 0001, 0010, 0100, 1000.
5. One now uses Pi to compute the occupation of acceptors.
from lh
from hh
EC
EV

## Slide 38: Number and Energy Considerations …
4N-4 States
In HH/LH bands
0000 1000 0100 0010 0001
[0000] is the charged state as it has N electrons, but N-1 protons.
Single hole configuration [0001] is uncharged, as we have N-1 electrons, and N-1 protons … same is true for [0010], [0100], [1000] states.
Going from [0000] to [0001] states, the number of electrons goes down by 1 (Ni=-1).
Going from [0000] to [0001] states energy goes down by –EA, because one electron is no longer occupying the high energy level at EA.

## Slide 39: Statistics of Acceptor Levels
0000 1000 0100 0010 0001
Steps 3 & 4
2N-2 states
00 10 01

## Slide 40: Filled and empty Donor/Acceptor Levels
0000 1000 0100 0010 0001
2N-2 states
00 10 01
4N-4 States
In HH/LH bands
(Two holes can not seat together)

## Slide 41: Distributions are physical …. Define an effective donor level
Degeneracy factor …
Effective donor level

## Slide 42: Carrier-density with Uniform Doping
A bulk material must be charge neutral over all …
Further if the doping is spatially homogenous
Once you know EF, you can calculate n, p, ND+, NA-.
(approx.)
FD integral vs. FD function ?

## Slide 43: Summary …
A bulk material must be charge neutral over all …
Further if the material is spatially homogenous

## Slide 44: Intrinsic Concentration

## Slide 45: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
14.1 Basic concepts of donors and acceptors
14.2 Statistics of donor and acceptor levels
14.3 Temperature dependence of carrier concentration
14.4 Multiple doping, co-doping, and heavy-doping
Video
Video
r0
=
Video
Video

## Slide 46: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
14.1 Basic concepts of donors and acceptors
14.2 Statistics of donor and acceptor levels
14.3 Temperature dependence of carrier concentration
14.4 Multiple doping, co-doping, and heavy-doping
Video
Video
r0
=
Video
Video

## Slide 47: Section 14 Doping
Solid State Devices
14.3 Temperature dependence of carrier concentration

## Slide 48: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
14.1 Basic concepts of donors and acceptors
14.2 Statistics of donor and acceptor levels
14.3 Temperature dependence of carrier concentration
14.4 Multiple doping, co-doping, and heavy-doping
Video
Video
r0
=
Video
Video

## Slide 49: Carrier Density with Donors
In spatially homogenous field-free region …
Assume
N-type doping …
n
(will plot in next slide)

## Slide 50: Temperature-dependent Concentration
Temperature
1
Freeze
out
Extrinsic
Intrinsic

## Slide 51: Physical Interpretation
Temperature
1
Freeze
out
Extrinsic
Intrinsic

## Slide 52: Electron Concentration with Donors

## Slide 53: Electron concentration with Donors
No approximation so far ….

## Slide 54: High Donor Density / Freeze out T
Temperature
1
Freeze
out
Extrinsic
Intrinsic

## Slide 55: Extrinsic T
Electron concentration equals donor density
hole concentration by nxp=ni2
Temperature
1
Freeze
out
Extrinsic
Intrinsic

## Slide 56: Intrinsic T
Temperature
1
Freeze
out
Extrinsic
Intrinsic
0

## Slide 57: Extrinsic/Intrinsic T
What will happen if you use silicon circuits at very high temperatures ?
Bandgap determines the intrinsic carrier density.
Temperature
1
Freeze
out
Extrinsic
Intrinsic

## Slide 58: Determination of Fermi-level
Temperature
1
Freeze
out
Extrinsic
Intrinsic

## Slide 59: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
14.1 Basic concepts of donors and acceptors
14.2 Statistics of donor and acceptor levels
14.3 Temperature dependence of carrier concentration
14.4 Multiple doping, co-doping, and heavy-doping
Video
Video
r0
=
Video
Video
Temperature
1
Freeze
out
Extrinsic
Intrinsic

## Slide 60: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
14.1 Basic concepts of donors and acceptors
14.2 Statistics of donor and acceptor levels
14.3 Temperature dependence of carrier concentration
14.4 Multiple doping, co-doping, and heavy-doping
Video
Video
r0
=
Video
Video
Temperature
1
Freeze
out
Extrinsic
Intrinsic

## Slide 61: Section 14 Doping
Solid State Devices
14.4 Multiple doping, co-doping, and heavy-doping

## Slide 62: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
14.1 Basic concepts of donors and acceptors
14.2 Statistics of donor and acceptor levels
14.3 Temperature dependence of carrier concentration
14.4 Multiple doping, co-doping, and heavy-doping
Video
Video
r0
=
Video
Video
Temperature
1
Freeze
out
Extrinsic
Intrinsic

## Slide 63: Multiple Donor Levels
Multiple levels of same donor …
Codoping…

## Slide 64: Heavy Doping Effects: Bandtail States
E
k
k ?
E

## Slide 65: Heavy Doping Effects: Hopping Conduction
E
k
Bandgap narrowing
Band transport
vs.
hopping-transport
e.g. Base of HBTs
K?
E
e.g. a-silicon, OLED

## Slide 66: Conclusions
Charge neutrality condition and law of mass-action allows calculation of Fermi-level and all carrier concentration.
For semiconductors with field, charge neutrality will not hold and we will need to use Poisson equation.
Heaving doping effects play an important role in carrier transport.

## Slide 67: Section 14 Doping
I = G x V
density
velocity
charge
area
= q x n x v x A
  Need to “move” the Fermi level
  ”add” electrons – n-type doping – EF close to Ec
  “add” holes – p-type doping – EF close to Ev
14.1 Basic concepts of donors and acceptors
14.2 Statistics of donor and acceptor levels
14.3 Temperature dependence of carrier concentration
14.4 Multiple doping, co-doping, and heavy-doping
Video
Video
r0
=
Video
Video