## Slide 1: Section 15 Introduction to Non-Equilibrium
Solid State Devices

## Slide 2: Section 15 Introduction to Non-Equilibrium
Transport with scattering, non-equilibrium Stat. Mech.
Drift-diffusion equation with recombination-generation
Understanding transport in devices
Diodes, BJT/HBT, MOS
Materials, composition, crystals
Tabulated for “known” bulk materials
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
I = G x V
density
velocity
charge
area
= q x n x v x A
How does the system
go BACK to
equilibrium?
15.1 Steady State, Transient, Equilibrium
15.2 Recombination & Generation Overview
I
Video
Video
Environment

## Slide 3: Equilibrium, Steady state, Transient
Device
Steady state
Equilibrium
time
(n,p)
Environment

## Slide 4: Equilibrium, Steady state, Transient
Device
Steady state
Transient
Equilibrium
time
(n,p)
time
(n,p)
Environment

## Slide 5: Detailed Balance: Simple Explanation
typical semiconductor device there are 1e17 to 1e20 electrons in the conduction band. All electrons carry charge and are occupying their respective DOS.
Equilibrium is a very active place
Fermi-Dirac distribution demands exploration of allowed states
In equilibrium each process is balanced by its counter process => Detailed Balance
=> Externally it looks as if nothing is happening.
This is different from steady state!!!
Mexico
China
India
USA
3
3
2
2
4
4
9 in & 9 out
All numbers are people/unit time.
Mexico
China
India
USA
4
6
3
2
4
5
1
1
Device
Equilibrium
Environment

## Slide 6: Detailed Balance: Simple Explanation
Device
Equilibrium
Environment
Equilibrium is a very active place
Fermi-Dirac distribution demands exploration of allowed states
In equilibrium each process is balanced by its counter process => Detailed Balance
=> Externally it looks as if nothing is happening for each site.
This is different from steady state!!!
Mexico
China
India
USA
3
3
2
2
4
4
The rates of exchange of people (particles) between every pair of countries (energy levels) is balanced. Hence the name “Detailed Balance”.
Detailed balance is the property of equilibrium
The population of each of the countries (energy levels) remains constant under detailed balance.
The concept of detailed balance is powerful, because it can be used for many things
derive particle distributions Fermi-Dirac, Bose-Einstein
reduce the number of unknown rate constants by half
9 in & 9 out from USA
All numbers are people/unit time.
Mexico
China
India
USA
4
6
3
2
4
5
1
1

## Slide 7: Steady State Response
Device
Equilibrium
Environment
Equilibrium is a very active place
Fermi-Dirac distribution demands exploration of allowed states
In equilibrium each process is balanced by its counter process => Detailed Balance
=> Externally it looks as if nothing is happening for each site.
This is different from steady state!!!
Mexico
China
India
USA
3
3
2
2
4
4
9 in & 9 out from USA
All numbers are people/unit time.
Mexico
China
India
USA
4
6
3
2
4
5
1
1
12 in and 12 out from USA
Disturbing the detailed balance requires non-equilibrium conditions (needs energy). Unidirectional forces (red lines) can create such
Non-equilibrium conditions
The population of a country (energy level) remains constant with time after steady state is reached.
4+1 in and 5 out from India
3+1 in and 5 out from Mexico
`
`
`

## Slide 8: Steady State Response
Device
Equilibrium
Environment
Equilibrium is a very active place
Fermi-Dirac distribution demands exploration of allowed states
In equilibrium each process is balanced by its counter process => Detailed Balance
=> Externally it looks as if nothing is happening for each site.
This is different from steady state!!!
Mexico
China
India
USA
3
3
2
2
4
4
9 in & 9 out from USA
All numbers are people/unit time.
Mexico
China
India
USA
4
6
3
2
4
5
1
1
12 in and 12 out from USA
Disturbing the detailed balance requires non-equilibrium conditions (needs energy). Unidirectional forces (red lines) can create such
Non-equilibrium conditions
The rates of exchange of people (particles)
between every pair of countries (energy
levels) is NOT balanced.
The population of a country (energy level) remains constant with time after steady state is reached.
`
`
`
`
`

## Slide 9: Steady State Response
Device
Equilibrium
Environment
Equilibrium is a very active place
Fermi-Dirac distribution demands exploration of allowed states
In equilibrium each process is balanced by its counter process => Detailed Balance
=> Externally it looks as if nothing is happening for each site.
This is different from steady state!!!
Mexico
China
India
USA
3
3
2
2
4
4
9 in & 9 out from USA
All numbers are people/unit time.
Mexico
China
India
USA
4
6
3
2
4
5
1
1
Disturbing the detailed balance requires non-equilibrium conditions (needs energy). Unidirectional forces (red lines) can create such
Non-equilibrium conditions
The rates of exchange of people (particles)
between every pair of countries (energy
levels) is NOT balanced.
The flux at steady state is balanced overall,
The population of a country (energy level) remains constant with time after steady state is reached.

## Slide 10: Steady State Response
Device
Equilibrium
Environment
Equilibrium is a very active place
Fermi-Dirac distribution demands exploration of allowed states
In equilibrium each process is balanced by its counter process => Detailed Balance
=> Externally it looks as if nothing is happening for each site.
This is different from steady state!!!
Mexico
China
India
USA
3
3
2
2
4
4
9 in & 9 out from USA
All numbers are people/unit time.
Mexico
China
India
USA
4
6
3
2
4
5
1
1
Disturbing the detailed balance requires non-equilibrium conditions (needs energy). Unidirectional forces (red lines) can create such
Non-equilibrium conditions
The rates of exchange of people (particles)
between every pair of countries (energy
levels) is NOT balanced.
The flux at steady state is balanced overall,
The population of a country (energy level) remains constant with time after steady state is reached.
One can use the requirement that net flux at steady state be zero to calculate steady state population of a country

## Slide 11: Transient Response
Equilibrium is a very active place
Fermi-Dirac distribution demands exploration of allowed states
In equilibrium each process is balanced by its counter process => Detailed Balance
=> Externally it looks as if nothing is happening for each site.
This is different from steady state!!!
Mexico
China
India
USA
3
3
2
2
4
4
9 in & 9 out from USA
All numbers are people/unit time.
Mexico
China
India
USA
4
6
3
2
4
5
1
1
=> Externally it looks as if nothing is happening for the overall system.
Disturbing the detailed balance requires non-equilibrium conditions (needs energy). Unidirectional forces (red lines) can create such
Non-equilibrium conditions
The rates of exchange of people (particles)
between every pair of countries (energy
levels) is NOT balanced.
The flux at steady state is balanced overall,
The population of a country (energy level) remains constant with time after steady state is reached.
One can use the requirement that net flux at steady state be zero to calculate steady state population of a country (Eq. 5.21)
Mexico
China
India
USA
3
5
3
4
5
1
1
2
Forced unidirectional connections
(red lines) disturbs equilibrium
(e.g. 10 in/12 out at time t1
local populations not conserved,
but global population is ….
Transient populations
I
Transport with scattering, non-equil, Stat. Mech.
Drift-diffusion eq. with recombination-generation
Understanding device transport
Diodes, BJT/HBT, MOS
Materials, composition, crystals
Tabulated for “known” bulk materials
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses

## Slide 12: Section 15 Introduction to Non-Equilibrium
Transport with scattering, non-equil, Stat. Mech.
Drift-diffusion eq. with recombination-generation
Understanding device transport
Diodes, BJT/HBT, MOS
Materials, composition, crystals
Tabulated for “known” bulk materials
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
I = G x V
density
velocity
charge
area
= q x n x v x A
How does the system
go BACK to
equilibrium?
15.1 Steady State, Transient, Equilibrium
  Critical conceptual differences!
  Need to understand these!
15.2 Recombination & Generation Overview
I
Video
Video
Mexico
China
India
USA
3
3
2
2
4
4
Mexico
China
India
USA
4
6
3
2
4
5
1
1
12 in 12 out
Population stabilized
Steady State But NOT Equilibrium

## Slide 13: Section 15 Introduction to Non-Equilibrium
Transport with scattering, non-equil, Stat. Mech.
Drift-diffusion eq. with recombination-generation
Understanding device transport
Diodes, BJT/HBT, MOS
Materials, composition, crystals
Tabulated for “known” bulk materials
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
I = G x V
density
velocity
charge
area
= q x n x v x A
How does the system
go BACK to
equilibrium?
15.1 Steady State, Transient, Equilibrium
  Critical conceptual differences!
  Need to understand these!
15.2 Recombination & Generation Overview
I
Video
Video
Mexico
China
India
USA
3
3
2
2
4
4
Mexico
China
India
USA
4
6
3
2
4
5
1
1
12 in 12 out
Population stabilized
Steady State But NOT Equilibrium

## Slide 14: Section 15 Introduction to Non-Equilibrium
Solid State Devices
15.2 Recombination & Generation Overview

## Slide 15: Section 15 Introduction to Non-Equilibrium
Transport with scattering, non-equil, Stat. Mech.
Drift-diffusion eq. with recombination-generation
Understanding device transport
Diodes, BJT/HBT, MOS
Materials, composition, crystals
Tabulated for “known” bulk materials
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
I = G x V
density
velocity
charge
area
= q x n x v x A
How does the system
go BACK to
equilibrium?
15.1 Steady State, Transient, Equilibrium
  Critical conceptual differences!
  Need to understand these!
15.2 Recombination & Generation Overview
I
Video
Video
Mexico
China
India
USA
3
3
2
2
4
4
Mexico
China
India
USA
4
6
3
2
4
5
1
1
12 in 12 out
Population stabilized
Steady State But NOT Equilibrium

## Slide 16: Indirect vs. Direct Bandgap
The top & bottom of bands do not align at
same wavevector k for indirect bandgap material

## Slide 17: Direct Band-to-band Recombination
Photon
GaAs, InP, InSb (3D)
Lasers, LEDs, etc.
In real space …
In energy space …
Photon
Direct transistion – direct gap material
e and h must have same wavelength 1 in 1,000,000 encounters

## Slide 18: Direct Excitonic Recombination
Photon (wavelength reduced from bulk)
CNT, InP, ID-systems
Transistors, Lasers, Solar cells, etc.
In energy space …
In real space …
Mostly in 1D systems
Requires strong coulomb interactions

## Slide 19: Indirect Recombination (Trap-assisted)
Phonon
Ge, Si, ….
Transistors, Solar cells, etc.
Trap needs to be mid-gap to be effective.
Cu or Au in Si
States close to Ec or Ev do not help efficiently.
Cu in Si is extremely efficient in providing recombination
Cu in Si was avoided completely for many years
Intel introduced Cu for interconnects – special precautions so Cu does not enter the Si.

## Slide 20: Indirect Recombination (Trap-assisted)
Phonon
Ge, Si, ….
Transistors, Solar cells, etc.
Trap needs to be mid-gap to be effective.
Cu or Au in Si
States close to Ec or Ev do not help efficiently.
Cu in Si is extremely efficient in providing recombination
Cu in Si was avoided completely for many years
Intel introduced Cu for interconnects – special precautions so Cu does not enter the Si.
Recombination rate is in general slower than direct via photon.
Why?
1 electron and one hole need to localize AND find a trap. … less likely event.

## Slide 21: Impact Ionization – A Generation Mechanism
Si, Ge, InP
Lasers, Transistors, etc.
4
3
1
2
Inverse of the Auger recombination
Requires very high electric field

## Slide 22: Auger Recombination
Phonon (heat)
InP, GaAs, …
Lasers, etc.
1
2
3
1
2
4
3
4
Requires very high electron density

## Slide 23: Photon Energy and Wavevector
Photon has large energy for excitation through bandgap,
but its wavevector is negligible compared to size of BZ
Si lattice

## Slide 24: Phonon Energy and Wavevector
Phonon has large wavevector comparable to BZ,
but negligible energy compared to bandgap
vsound ~ 103 m/s << vlight=c ~ 106m/s
lsound >> llight

## Slide 25: Localized Traps and Wavevector
Trap provides the wavevector
necessary for indirect transition
a

## Slide 26: Conclusions
Concepts of equilibrium, steady state, and transient dynamics should be clearly understood.
There are wide variety of generation-recombination events that allow restoration of equilibrium once the stimulus is removed.
Direct recombination is photon-assisted, indirect recombination phonon assisted.
Mexico
China
India
USA
3
3
2
2
4
4
Mexico
China
India
USA
4
6
3
2
4
5
1
1
12 in 12 out
Population stabilized
Steady State But NOT Equilibrium

## Slide 27: Section 15 Introduction to Non-Equilibrium
Transport with scattering, non-equil, Stat. Mech.
Drift-diffusion eq. with recombination-generation
Understanding device transport
Diodes, BJT/HBT, MOS
Materials, composition, crystals
Tabulated for “known” bulk materials
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
I = G x V
density
velocity
charge
area
= q x n x v x A
How does the system
go BACK to
equilibrium?
15.1 Steady State, Transient, Equilibrium
15.2 Recombination & Generation Overview
I
Video
Video
Mexico
China
India
USA
3
3
2
2
4
4
Mexico
China
India
USA
4
6
3
2
4
5
1
1
12 in 12 out
Population stabilized
Steady State But NOT Equilibrium

## Slide 28: Section 15 Introduction to Non-Equilibrium
Understanding device transport
Diodes, BJT/HBT, MOS
Materials, composition, crystals
Tabulated for “known” bulk materials
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
I = G x V
density
velocity
charge
area
= q x n x v x A
How does the system
go BACK to
equilibrium?
15.1 Steady State, Transient, Equilibrium
15.2 Recombination & Generation Overview
I
Video
Video
Mexico
China
India
USA
3
3
2
2
4
4
Mexico
China
India
USA
4
6
3
2
4
5
1
1
12 in 12 out
Population stabilized
Steady State But NOT Equilibrium
Transport with scattering, non-equil, Stat. Mech.
Drift-diffusion eq. with recombination-generation
Section 16 Recombination & Generation