## Slide 1: Tight-Binding Modeling of Intermediate Valence Compound SmSe for Piezoelectronic Devices
Zhengping Jiang*, Yaohua Tan, Micheal Povolotskyi,
Tillmann Kubis, Gerhard Klimeck (Purdue University)
Marcelo Kuroda, Dennis Newns, Glenn Martyna (IBM)
Timothy Boykin (The University of Alabama in Huntsville)
*jiang32@purdue.edu

## Slide 2: Outline
Motivation
  Beyond Moore’s Law
  Next Generation Switch
Piezoelectronic Transistor
  Device Design
  Working Principle
Metal Insulator Transition in SmSe
Tight Binding Parameterization
Summary

## Slide 3: Beyond Moore’s Law
Heat dissipation prevents any performance improvement through increasing clock frequency!
Thinking Beyond Moore’s Law → Beyond Si FET
Technology drives device to scaling limit.
Latest Generation FinFET
60mV/dec barrier still exist

## Slide 4: Next Switch
Energy Filtering
Internal Voltage Step-up
Internal Transduction
TFET
Ferroelectronic FET & quantum capacitive device
Spin fet & nano-electromechanical switch
Low Subthreshold Swing → Circumvent the Boltzmann distribution or break the direct voltage-barrier relation
Quantum tunneling instead of thermal emission
Lower voltage to flip spin then modulate barrier height

## Slide 5: Piezoelectronic Transistor (PET)
Energy Filtering
Internal Voltage Step-up
Internal Transduction
PiezoResistive Material
(e.g. SmSe)
Relaxor PiezoElectric Material (e.g. PMN-PT)
2 Channels
3 Contacts
Voltage INPUT
Current OUTPUT
Properties of PE and PR enable internal voltage step-up and internal transduction of acoustic and electrical signals.
Pressure induced metal insulator transition
Deformation due to E field

## Slide 6: Working principle
Internal Voltage Step-up
Internal Transduction
Pressure
on PR
PR: insulator to metal transition
Deformation
Gate Voltage
Vg
How does PET achieve SS<60mV/dec?
Voltage applied on Gate – Common terminals:
Deformation inside PE channel
Electrical → Acoustic
Vg
Current in PE channel
Acoustic → Electrical

## Slide 7: Mechanical and Electrical Features
SmSe
Phys. Rev. Lett. 25, 1430 (1970)
Internal Transduction
Internal Voltage Step-up
D. M. Newns, B. G. Elmegreen, X. H. Liu and G. J. Martyna, Advanced Materials (2012).
PET is capable of high performance and large scale integration!
Large Area / Volume Ratio Between PE/PR
Hammer-Nail Effect
Small Deformation in PE → Large Strain in PR
High response PE and big conductance change in PR
High response Relaxor Piezoelectric Material
Sound velocity in nanostructure → high speed
Small Volume Change → Big Resistivity Change in PR

## Slide 8: Metal-Insulator Transition in SmSe
Conventional Ec
Conventional Ev
5d
4p
4f
Eg = 0.45eV
5d
4p
4f
Pressure
Insulating material
Conducting material
Scaling limit of PET determined by onset of tunneling.
Quantum transport for MIT in tight-binding.
f-electron band, New Ev

## Slide 9: Methods
1. ab-initio calculation
2. Determine TB model and fitting variables
→ Analytical formula for TB basis functions is Tesseral function, is to be parameterized
Ab-initio band structure Ei(k)
Wave functions
GGA + U
3. Iteratively optimization
DFT Hamiltonian to TB Hamiltonian: basis transformation
Hab-initio  HTB
Approximate HTB by two center integrals
Compare Ek with DFT and redo Step 3.
Parameter refinement by simplex method
→ Target: Ek along high symmetry directions

## Slide 10: Determine tight binding model
Require TB model: sp3d5f7s* + SO
SmSe: DFT bandstructure
DFT decomposition: DOS into angular momentum
Se p-orbital: lower valence band
Sm d-orbital: conduction band
Sm f-orbital: top valence band
Splitting of f-orbital: covered through SO coupling
DFT density of states:
f-electron splitting due to strong correlation

## Slide 11: Strain effects on bandstructure of SmSe
Bandgap is closing with strain in linear trend
TB matches DFT trend!
Bandstructure without strain
Energy range most relevant to transport
Energy range most relevant to transport
Parameter fitted to band structure of hydrostatic strain and applied to clamped (uniaxial) strain with no modification.

## Slide 12: Transport simulation
PR layer is measured in thin film.
Lateral length > Thickness
Simulation is approximated by 1-D model.
Extract 1-D simulation model with and without electric field.
Periodic BC

## Slide 13: Results
Modeled imaginary band (b) and transmission (c) of SmSe thin film.

## Slide 14: Summary
Piezoelectronic Transistor shows promising properties to overcome 60mV/dec limit.
  Internal transduction
  Internal “voltage” step-up
Metal-Insulator Transition in piezoresistive material is critical
Tight binding model could reproduce MIT from bandstructure effects
  Second nearest neighbor TB model: sp3d5f7s*+SO
  Strain model
Need modeling of Metal-SmSe interface and e-e scattering for f-electrons (work in progress)

## Slide 15
THANKS

## Slide 16: Method
Step: ab-initio calculation  Ei(k), φi,k(r), Hab-initio
2. Step: Define analytical formula for TB basis functions n,l,m (r,,) = Rn,l(r)Yl,m(,) Yl,m(,) is Tesseral function, Rn,l(r) is to be parametrized
Ab-initio band structure Ei(k)
Wave functions φi,k(r)
Yl,m(θ,φ)

## Slide 17: Method (continue)
4. Step:
basis transformation (low rank approximation):
Hab-initio  HTB
Approximate HTB by two center integrals;
Step:
Compare the TB results (band structure, wave functions) to ab-initio results; Measure the overlaps of basis functions;
J. Slater & G.Koster PR. 94,1498(1964)
A. Podolskiy & P. Vogl PRB 69, 233101 (2004)
Iteratively optimize the TB results
Step: Parameterize
get transform matrix U: ab-initio basis  TB basis
Step：
Parameter refinement by simplex method
→ Target: Ek along high symmetry directions