## Slide 1
Objective:
Calculate phonon-limited injection velocity vinj and ballisticity at the top-of-the barrier in n-type Si and InAs and p-type Si and Ge NW FETs with different oritentations
Approach:
Tight-binding (sp3d5s*) description of the electron/hole properties
Atomistic Representation of the NWs
Quantized phonon dispersion (VFF)
Quantum transport with NEGF
Results and Impacts:
vinj as function of the charge density at the top-of-the-barrier
[100] InAs NW highest electron velocity and close to ballistic limit
[110] Ge NW highest hole velocity, but 50-60% of ballistic limit
Injection Velocity in Si, Ge, and InAs NW FETs Mathieu Luisier and Gerhard Klimeck IEDM 2010
[100]
[110]
[111]
Si NW FET
structure
Caption: Phonon-limited electron (left) and hole (right) injection velocity in Si, Ge, and InAs NW FETs