## Slide 1: Antiferroelectricity
Aidan Broy

## Slide 2: Dipole Review
3 main types of polarization: orientational, ionic, and electronic
Dipole reaction to an electric field
  Regular dielectric: Statistical bias to align to field
  Ferroelectric: Full alignment past coercive field
  Antiferroelectric: Anti-parallel alignment
Regular Dielectric (w/ internal dipole)
Ferroelectric
Antiferroelectric

## Slide 3: Polarization Density Comparison
Linear: Dielectric without internal dipole only experiences electronic polarization
Ferroelectric: Leap near E=0 because of orientational polarization
Antiferroelectric: Leaps after electric field reaches critical field
[1]

## Slide 4: What Causes AFE?
Visualize with Landau-Ginzburg-Devonshire Formula
  AFE materials have structural coupling that can be modeled as a P6 term
Phonon’s frequency can “soften” to 0 and induce new structure.
  Reduced influence from x2 leads to two valleys
  Coupling energies force neighboring molecules into opposite valleys
E = aP2 +bP4 +cP6
Polarization Density
Free Energy
FE structural coupling
AFE structural coupling
Cooled

## Slide 5: AFE Materials
Ideal AFE material:
  Low transition field
  Safe to use
  High dielectric constant
Examples:
  BaTiO3’s transition field causes dielectric breakdown if undoped [2]
  PbZrO3 has lead, so not suitable for some applications [3]
Surface SEM pictures of PLZT antiferroelectric films with different thickness [3]

## Slide 6: Applications - Capacitor
Capacitors have higher output than batteries, but traditionally lower capacity
AFE material often has the most recoverable energy
  Not much total energy stored in linear material
  Not all energy recoverable from FE material
All from [1]

## Slide 7: Applications - Memory
By introducing an internal bias, we can make the AFE act like a FE
  Chemical potential gradient leads to charge build up on interfaces
  Only works for thin films
AFE materials can function for more cycles than FE materials
RuOx (W=5.3eV)
ZrO2
TiN (W=4.5eV)
TiN-ZrO2-TiN (dotted) and RuOx-ZrO2-TiN (solid) polarization vs voltage and energy [4]

## Slide 8: AFE Modes
High Electric Field (1, 3)
Low Electric Field (2)
3
2
1
1
3
2
AFE hysteresis loop [6]
Polarization Density
Free Energy

## Slide 9: Conclusion
AFEs are a group of materials with antiparallel dipole orientation
Applications: energy storage, memory, and more
Future work: finding suitable, synthesizable materials
[5]

## Slide 10: Bibliography
[1] Z. Liu, T. Lu, J. Ye, G. Wang, X. Dong, R. Withers, and Y. Liu, "Antiferroelectrics for energy storage applications: A review," Advanced Materials Technologies, vol. 3, no. 9, p. 1800111, Sep. 2018. doi: 10.1002/admt.201800111.
[2] A. Jain et al., "Antiferroelectric materials review," Journal of Alloys and Compounds, vol. 909, 2022. doi: 10.1016/j.jallcom.2021.163165.
[3] X. Hao, J. Zhai, F. Zhou, X. Song, and S. An, "Thickness and frequency dependence of electric-field-induced strains of sol-gel derived (Pb0.97La0.02)(Zr0.95Ti0.05)O3 antiferroelectric films," Journal of Sol-Gel Science and Technology, vol. 53, pp. 366–371, Feb. 2010. doi: 10.1007/s10971-009-2104-1.
[4] M. Pešić, M. Hoffmann, C. Richter, T. Mikolajick, and U. Schroeder, "Nonvolatile random access memory and energy storage based on antiferroelectric like hysteresis in ZrO2," Advanced Functional Materials, vol. 26, no. 41, pp. 7486–7494, 2016. doi: 10.1002/adfm.201603182.
[5] C. A. Randall, Z. Fan, I. Reaney, L.-Q. Chen, and S. Trolier-McKinstry, "Antiferroelectrics: History, fundamentals, crystal chemistry, crystal structures, size effects, and applications," Journal of the American Ceramic Society, vol. 104, no. 8, pp. 3775–3810, 2021. doi: 10.1111/jace.17834.
[6] IEEE:Electrical4U, "Antiferroelectricity," Electrical4U, May 15, 2024. [Online]. Available: https://www.electrical4u.com/antiferroelectricity/.