## Slide 1: ECE 60658 : Anomalous Hall Effect
Ho Jun Lee (David)
First year Electrical Engineering as MS

## Slide 2: Historical Background
1879 Ordinary Hall Effect
Edwin Hall discovers transverse voltage in non-magnetic conductors under magnetic field B
1881 Anomalous Hall Effect
Hall observes the effect is ~10x larger in ferromagnetic iron without needing B
1954 Luttinger & Karplus
First intrinsic mechanism proposed – band structure origin via spin-orbit coupling
2010 Nagaosa et al. (RMP)
Landmark review unifying all mechanism through Berry curvature framework

## Slide 3: Ordinary vs Anomalous Hall Effect
Ordinary Hall Effect (OHE)
Origin | Lorentz force on charge carries
Requires | External magnetic field B
Hall resistivity | 𝜌xy = RoB
Material | Any conductor
Mechanism | Classical – single carrier deflection
Anomalous Hall Effect (AHE)
Origin | Spin-orbit coupling + broken time-reversal
Requires | Magnetic order (no external B needed)
Hall resistivity | 𝜌xy = RoB + RsM
Material | Ferromagnets & topological materials
Mechanism | Quantum – Berry curvature & scattering
General Hall Resistivity : 𝜌xy = RoB + RsM where Rs = Anomalous Hall coefficient

## Slide 4: Three Mechanism of AHE
Intrinsic
Skew Scattering
Side Jump
Origin : Band structure / Berry curvature
Regime : Moderate conductivity
Oxysj = oxx0(Independent)
Oxysk = oxx (Linear)
Origin : Asymmetric impurity scattering
Regime : High conductivity (clean limit)
Origin : Transverse shift during scattering
Regime : Intermediate/dirty regime
Anomalous velocity from Berry curvature in k-space. Does NOT require impurities.
Topological in origin
Dominates in most metallic ferromagnets
SOC causes left-right asymmetry in scattering probability. Spin-up and spin-down scatter differently
Dominates in ultra-clean, high-conductivity samples
Electrons undergo a sudden transverse displacement y ~ 1A during each scattering event.
Often smaller, harder to isolate experimentally
Reference: Nagaosa, Sinova et al., Rev. Mod. Phys. 82, 1549 (2010)

## Slide 5: Experimental Evidence
Material | Oxy (S/cm) | Mechanism | Notes
Fe (bcc) | ~750 | Intrinsic | Transition metal benchmark, Berry curvature maps well with ab initio
Co (hcp) | ~480 | Intrinsic | Good agreement with first-principles Berry curvature calc.
Ni (fcc) | ~200 | Intrinsic/Skew | Mixed mechanism, skew scattering non-negligible
CuCr2Se4 | ~3200 | Intrinsic | Spinel; confirmed pxy = p2 scaling (Lee et al. 2004)
Co3Sn2S2 | ~1130 | Intrinsic | Magnetic Weyl semimetal; Fermi arc surface states
MnxGa1-xAs | Varies | Intrinsic/Skew | Dilute magnetic semiconductor; gate-tunable AHE
Reference: Nagaosa et al. RMP 2010; Lee et al. PRL 2004; Liu et al. Nano Lett. 2020

## Slide 6: Applications
Spintronics Devices
  AHE enables reading magnetic state without external B field. Used in magnetic sensors and read heads
MRAM (Spin-orbit Torque)
  Spin Hall + AHE detect and switch magnetization. SOT-MRAM is faster and more efficient than STT-MRAM
Topological Material Probe
  AHE is strong for ferromagnetism and Weyl fermions. Used to detect topological phase transitons
Quantum Anomalous Hall (QAHE)
  Quantized AHE at zero B – observed in Cr-doped (BiSb)2Te3., platform for dissipation less edge transport
Antiferromagnetic Spintronics
  AHE in noncollinear AFMs (Mn3Sn) opens ultrafast Thz spintronic devices without stray fields
Topological Computing
  Berry curvature engineering in 2D magnets (Crl3, Fe3GeTe2) for future topological quantum computing