## Slide 1: Section 2 Materials
Gerhard Klimeck
gekco@purdue.edu
Solid State Devices
Notes: In..

## Slide 2: Section 2 Materials
2.1 Typical Semiconducting Materials
  Current flow in semiconductors (reminder)
  Elemental semiconductors in the periodic table
  Bonding for half-filled shells, column IV, III-V, and II-VI
2.2 Typical applications of elemental and compound semiconductors
2.3 Atomic Positions and Bond Orientations
  Solid State vs. other crystals
  Typical Atomic Arrangements in MOSFETS
Reference: Vol. 6, Ch. 1
2
One Video Segment
One Video Segment
One Video Segment
V
I

## Slide 3: Section 2 Typical Semiconducting Materials
V
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Quantum Mechanics + Equilibrium Statistical Mechanics
Concepts of effective masses and occupation factors
Transport with scattering, non-equilibrium Statistical Mechanics
Drift-diffusion equation with recombination-generation
I
Understanding transport in concrete devices
Diodes, BJT/HBT, MOS
I = G x V
density
velocity
charge
area
= q x n x v x A

## Slide 4: Section 2 Typical Semiconducting Materials
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Quantum Mechanics + Equilibrium Statistical Mechanics
Concepts of effective masses and occupation factors
Transport with scattering, non-equilibrium Statistical Mechanics
Drift-diffusion equation with recombination-generation
Understanding transport in concrete devices
Diodes, BJT/HBT, MOS
Atomic composition
- number of electrons per atom
Arrangement of atoms
- not all electrons are available for conduction

## Slide 5: Elemental Semiconductors in the Periodic Table
1) https://en.wikipedia.org/wiki/Periodic_table
Filling of electron shells
Increasing weight & size
Adding electron shells
Increasing weight & size
Si & Ge
Elemental semiconductors
IV =4
s&p shells
half-filled
VIII =8 shells
full
Atomic composition
- number of electrons per atom
Arrangement of atoms
- not all electrons are available for conduction

## Slide 6: s & p Orbital Shell Filling
1) https://en.wikipedia.org/wiki/Periodic_table
VIII =8 shells
full
IV =4
s&p shells
half-filled
II =2 s&p shell
filling
II =2 s&p shell
filling
Si & Ge
Elemental semiconductors
Filling of electron shells
Increasing weight & size
Adding electron shells
Increasing weight & size

## Slide 7: Focus on Columns II – VI in Periodic Table
1) https://en.wikipedia.org/wiki/Periodic_table
VIII =8 shells
full
IV =4
s&p shells
half-filled
II =2 s&p shell
filling
II =2 s&p shell
filling
Si & Ge
Elemental semiconductors
Filling of electron shells
Increasing weight & size
Adding electron shells
Increasing weight & size

## Slide 8: Focus on Columns II – VI in Periodic Table
1) https://en.wikipedia.org/wiki/Periodic_table
IV =4
s&p shells
half-filled
II =2 s&p shell
filling
Si & Ge
Elemental semiconductors
Filling of electron shells
Increasing weight & size
Adding electron shells
Increasing weight & size

## Slide 9: Focus on Columns II – VI in Periodic Table
1) https://en.wikipedia.org/wiki/Periodic_table
IV =4
s&p shells
half-filled
II =2 s&p shell
filling
Si & Ge
Elemental semiconductors
Filling of electron shells
Increasing weight & size
Adding electron shells
Increasing weight & size

## Slide 10: Focus on Columns II – VI in Periodic Table
1) https://en.wikipedia.org/wiki/Periodic_table
IV =4
s&p shells
half-filled
II =2 s&p shell
filling
Si & Ge
Elemental semiconductors
Adding electron shells
Increasing weight & size
Filling of electron shells

## Slide 11: Bonding for Half-Filled Shells – IV, III-V, II-VI
1) https://en.wikipedia.org/wiki/Periodic_table
IV =4
s&p shells
half-filled
II=4-2
Si & Ge
Elemental semiconductors
VI=4+2
Compound semiconductors
Adding electron shells
Increasing weight & size
Filling of electron shells
III=4-1
V=4+1
III-V
II-VI

## Slide 12: Section 2 Materials
plastic crystals
specific position
random orientation
solid crystals
specific position
specific orientation
2.1 Typical Semiconducting Materials
  Current flow in semiconductors (reminder)
  Elemental semiconductors in the periodic table
  Bonding for half-filled shells, column IV, III-V, and II-VI
2.2 Typical applications of elemental and compound semiconductors
2.3 Atomic Positions and Bond Orientations
  Solid State vs. other crystals
  Typical Atomic Arrangements in MOSFETS
Reference: Vol. 6, Ch. 1
One Video Segment
One Video Segment
One Video Segment

## Slide 13: Section 2 Materials
plastic crystals
specific position
random orientation
solid crystals
specific position
specific orientation
2.1 Typical Semiconducting Materials
  Current flow in semiconductors (reminder)
  Elemental semiconductors in the periodic table
  Bonding for half-filled shells, column IV, III-V, and II-VI
2.2 Typical applications of elemental and compound semiconductors
2.3 Atomic Positions and Bond Orientations
  Solid State vs. other crystals
  Typical Atomic Arrangements in MOSFETS
Reference: Vol. 6, Ch. 1
One Video Segment
One Video Segment
One Video Segment

## Slide 14: Section 2 Materials 2.2 Typical applications of elemental and compound semiconductors
Gerhard Klimeck
gekco@purdue.edu
Solid State Devices
Notes: In..

## Slide 15: Section 2 Materials
plastic crystals
specific position
random orientation
solid crystals
specific position
specific orientation
2.1 Typical Semiconducting Materials
  Current flow in semiconductors (reminder)
  Elemental semiconductors in the periodic table
  Bonding for half-filled shells, column IV, III-V, and II-VI
2.2 Typical applications of elemental and compound semiconductors
2.3 Atomic Positions and Bond Orientations
  Solid State vs. other crystals
  Typical Atomic Arrangements in MOSFETS
Reference: Vol. 6, Ch. 1
One Video Segment
One Video Segment
One Video Segment

## Slide 16: Applications of Elemental Semiconductors
Elemental (e.g., Si, Ge, C)
Si: Transistors - $260billion industry
1) "Crystal Viewer Lab (New Interactive Front End), https://nanohub.org/resources/crystalviewer
2) © Gerhard Klimeck
3) https://commons.wikimedia.org/wiki/File:Microprocessore_silicio_germano.jpg
4) https://commons.wikimedia.org/wiki/File:Interband_optical_transition.svg
5) https://commons.wikimedia.org/wiki/File:Hgcdte_bandgap_x_t.png
6) https://en.wikipedia.org/wiki/Lead(II)_sulfide https://en.wikipedia.org/wiki/File:Sulfid_olovnat%C3%BD.PNG
1)

## Slide 17: Applications of Elemental Semiconductors Compounds
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
Si: Transistors - $260billion industry
1) "Crystal Viewer Lab (New Interactive Front End), https://nanohub.org/resources/crystalviewer
2) © Gerhard Klimeck
3) https://commons.wikimedia.org/wiki/File:Microprocessore_silicio_germano.jpg
4) https://commons.wikimedia.org/wiki/File:Interband_optical_transition.svg
5) https://commons.wikimedia.org/wiki/File:Hgcdte_bandgap_x_t.png
6) https://en.wikipedia.org/wiki/Lead(II)_sulfide https://en.wikipedia.org/wiki/File:Sulfid_olovnat%C3%BD.PNG
1)
2)
SiGe is a random alloy!
No long-range order
Interfaces are NOT atomically flat
Adding electron shells
Increasing weight & size
NOT a uniform bond length

## Slide 18: Applications of Elemental Semiconductors Compounds
=> Bandgaps, effective masses, mobility….
Strained bonds => modified “electron sharing” => modified electronic properties
Top layer has a different natural lattice constant => get strained to fit!
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
SiGe: stressors
SiC: radiation
Si: Transistors - $260billion industry
1) "Crystal Viewer Lab (New Interactive Front End), https://nanohub.org/resources/crystalviewer
2) © Gerhard Klimeck
3) https://commons.wikimedia.org/wiki/File:Microprocessore_silicio_germano.jpg
4) https://commons.wikimedia.org/wiki/File:Interband_optical_transition.svg
5) https://commons.wikimedia.org/wiki/File:Hgcdte_bandgap_x_t.png
6) https://en.wikipedia.org/wiki/Lead(II)_sulfide https://en.wikipedia.org/wiki/File:Sulfid_olovnat%C3%BD.PNG
1)
3)
Adding electron shells
Increasing weight & size
2)

## Slide 19: Applications of III-V Compound Semiconductors
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
III-V: InP, GaAs, (InxGa 1-x)(AsyP 1-y)
Light Emitting Diodes, Lasers, Detectors
expensive
SiGe: stressors
SiC: radiation
Si: Transistors - $260billion industry
1) "Crystal Viewer Lab (New Interactive Front End), https://nanohub.org/resources/crystalviewer
2) © Gerhard Klimeck
3) https://commons.wikimedia.org/wiki/File:Microprocessore_silicio_germano.jpg
4) https://commons.wikimedia.org/wiki/File:Interband_optical_transition.svg
5) https://commons.wikimedia.org/wiki/File:Hgcdte_bandgap_x_t.png
6) https://en.wikipedia.org/wiki/Lead(II)_sulfide https://en.wikipedia.org/wiki/File:Sulfid_olovnat%C3%BD.PNG
2)
1)
3)
4)
Different bandgaps
=> Heterostructure engineering => Artificial atoms with custom designed wavelengths

## Slide 20: Applications of II-VI Compound Semiconductors
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
III-V: InP, GaAs, (InxGa 1-x)(AsyP 1-y)
II-VI: Hg1-xCdxTe
Far IR detectors
Soft and difficult
Light Emitting Diodes, Lasers, Detectors
expensive
SiGe: stressors
SiC: radiation
Si: Transistors - $260billion industry
1) "Crystal Viewer Lab (New Interactive Front End), https://nanohub.org/resources/crystalviewer
2) © Gerhard Klimeck
3) https://commons.wikimedia.org/wiki/File:Microprocessore_silicio_germano.jpg
4) https://commons.wikimedia.org/wiki/File:Interband_optical_transition.svg
5) https://commons.wikimedia.org/wiki/File:Hgcdte_bandgap_x_t.png
6) https://en.wikipedia.org/wiki/Lead(II)_sulfide https://en.wikipedia.org/wiki/File:Sulfid_olovnat%C3%BD.PNG
2)
1)
3)
4)
5)
Temperature (K)
Composition x
Bandgap (eV)

## Slide 21: Lead Sulfide – PbS – is different!
1) "Crystal Viewer Lab (New Interactive Front End), https://nanohub.org/resources/crystalviewer
2) © Gerhard Klimeck
3) https://commons.wikimedia.org/wiki/File:Microprocessore_silicio_germano.jpg
4) https://commons.wikimedia.org/wiki/File:Interband_optical_transition.svg
5) https://commons.wikimedia.org/wiki/File:Hgcdte_bandgap_x_t.png
6) https://en.wikipedia.org/wiki/Lead(II)_sulfide https://en.wikipedia.org/wiki/File:Sulfid_olovnat%C3%BD.PNG
Outlier from the column IV balance!
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
III-V: InP, GaAs, (InxGa 1-x)(AsyP 1-y)
IV-VI: PbS
II-VI: Hg1-xCdxTe
First semiconductor diodes
Very soft and difficult
Far IR detectors
Soft and difficult
Light Emitting Diodes, Lasers, Detectors
expensive
SiGe: stressors
SiC: radiation
Si: Transistors - $260billion industry
2)
1)
3)
4)
5)
6)

## Slide 22: Applications of Semiconductors
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
III-V: InP, GaAs, (InxGa 1-x)(AsyP 1-y)
IV-VI: PbS
II-VI: Hg1-xCdxTe
First semiconductor diodes
Very soft and difficult
Far IR detectors
Soft and difficult
Light Emitting Diodes, Lasers, Detectors
expensive
SiGe: stressors
SiC: radiation
Si: Transistors - $260billion industry
1) "Crystal Viewer Lab (New Interactive Front End), https://nanohub.org/resources/crystalviewer
2) © Gerhard Klimeck
3) https://commons.wikimedia.org/wiki/File:Microprocessore_silicio_germano.jpg
4) https://commons.wikimedia.org/wiki/File:Interband_optical_transition.svg
5) https://commons.wikimedia.org/wiki/File:Hgcdte_bandgap_x_t.png
6) https://en.wikipedia.org/wiki/Lead(II)_sulfide https://en.wikipedia.org/wiki/File:Sulfid_olovnat%C3%BD.PNG
2)
1)
3)
4)
5)
6)

## Slide 23: Materials are the Toolbox for Devices
plastic crystals
specific position
random orientation
First semiconductor diodes
Very soft and difficult
Far IR detectors
Soft and difficult
Light Emitting Diodes, Lasers, Detectors
expensive
SiGe: stressors
SiC: radiation
Si: Transistors - $260billion industry
Columns II-VI build a “Lego-like” tool box for semiconductor Devices
Chemical differences lead to different bandgaps
Physical lattice mismatch leads to strain
  Can be design feature or a physical instability
Not all combinations possible:
  lattice mismatch, room temperature instability
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
III-V: InP, GaAs, (InxGa 1-x)(AsyP 1-y)
IV-VI: PbS
II-VI: Hg1-xCdxTe
1) "Crystal Viewer Lab (New Interactive Front End), https://nanohub.org/resources/crystalviewer
2) © Gerhard Klimeck
3) https://commons.wikimedia.org/wiki/File:Microprocessore_silicio_germano.jpg
4) https://commons.wikimedia.org/wiki/File:Interband_optical_transition.svg
5) https://commons.wikimedia.org/wiki/File:Hgcdte_bandgap_x_t.png
6) https://en.wikipedia.org/wiki/Lead(II)_sulfide https://en.wikipedia.org/wiki/File:Sulfid_olovnat%C3%BD.PNG
2)
1)
3)
4)
5)
6)
solid crystals
specific position
specific orientation

## Slide 24: Section 2 Materials
plastic crystals
specific position
random orientation
Light Emitting Diodes, Lasers, Detectors
expensive
SiGe: stressors
SiC: radiation
Si: Transistors - $260billion industry
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
III-V: InP, GaAs, (InxGa 1-x)(AsyP 1-y)
IV-VI: PbS
II-VI: Hg1-xCdxTe
2)
1)
3)
4)
5)
6)
solid crystals
specific position
specific orientation
2.1 Typical Semiconducting Materials
  Current flow in semiconductors (reminder)
  Elemental semiconductors in the periodic table
  Bonding for half-filled shells, column IV, III-V, and II-VI
2.2 Typical applications of elemental and compound semiconductors
2.3 Atomic Positions and Bond Orientations
  Solid State vs. other crystals
  Typical Atomic Arrangements in MOSFETS
Reference: Vol. 6, Ch. 1
One Video Segment
One Video Segment
One Video Segment

## Slide 25: Section 2 Materials
plastic crystals
specific position
random orientation
Light Emitting Diodes, Lasers, Detectors
expensive
SiGe: stressors
SiC: radiation
Si: Transistors - $260billion industry
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
III-V: InP, GaAs, (InxGa 1-x)(AsyP 1-y)
IV-VI: PbS
II-VI: Hg1-xCdxTe
2)
1)
3)
4)
5)
6)
solid crystals
specific position
specific orientation
2.1 Typical Semiconducting Materials
  Current flow in semiconductors (reminder)
  Elemental semiconductors in the periodic table
  Bonding for half-filled shells, column IV, III-V, and II-VI
2.2 Typical applications of elemental and compound semiconductors
2.3 Atomic Positions and Bond Orientations
  Solid State vs. other crystals
  Typical Atomic Arrangements in MOSFETS
Reference: Vol. 6, Ch. 1
One Video Segment
One Video Segment
One Video Segment

## Slide 26: Section 2 Materials 2.3 Atomic Positions and Bond Orientations
Gerhard Klimeck
gekco@purdue.edu
Solid State Devices
Notes: In..

## Slide 27: Section 2 Materials
plastic crystals
specific position
random orientation
Light Emitting Diodes, Lasers, Detectors
expensive
SiGe: stressors
SiC: radiation
Si: Transistors - $260billion industry
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
III-V: InP, GaAs, (InxGa 1-x)(AsyP 1-y)
IV-VI: PbS
II-VI: Hg1-xCdxTe
2)
1)
3)
4)
5)
6)
solid crystals
specific position
specific orientation
2.1 Typical Semiconducting Materials
  Current flow in semiconductors (reminder)
  Elemental semiconductors in the periodic table
  Bonding for half-filled shells, column IV, III-V, and II-VI
2.2 Typical applications of elemental and compound semiconductors
2.3 Atomic Positions and Bond Orientations
  Solid State vs. other crystals
  Typical Atomic Arrangements in MOSFETS
Reference: Vol. 6, Ch. 1
One Video Segment
One Video Segment
One Video Segment

## Slide 28: Spatial Atomic Arrangements Position and Bond Orientation
plastic crystals
specific position
random orientation
First semiconductor diodes
Very soft and difficult
Far IR detectors
Soft and difficult
Light Emitting Diodes, Lasers, Detectors
expensive
SiGe: stressors
SiC: radiation
Si: Transistors - $260billion industry
Columns II-VI build a “Lego-like” tool box for semiconductor Devices
Chemical differences lead to different bandgaps
Physical lattice mismatch leads to strain
  Can be design feature or a physical instability
Not all combinations possible:
  lattice mismatch, room temperature instability
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
III-V: InP, GaAs, (InxGa 1-x)(AsyP 1-y)
IV-VI: PbS
II-VI: Hg1-xCdxTe
1) "Crystal Viewer Lab (New Interactive Front End), https://nanohub.org/resources/crystalviewer
2) © Gerhard Klimeck
3) https://commons.wikimedia.org/wiki/File:Microprocessore_silicio_germano.jpg
4) https://commons.wikimedia.org/wiki/File:Interband_optical_transition.svg
5) https://commons.wikimedia.org/wiki/File:Hgcdte_bandgap_x_t.png
6) https://en.wikipedia.org/wiki/Lead(II)_sulfide https://en.wikipedia.org/wiki/File:Sulfid_olovnat%C3%BD.PNG
2)
1)
3)
4)
5)
6)
solid crystals
specific position
specific orientation

## Slide 29: Spatial Atomic Arrangements Position and Bond Orientation
solid crystals
plastic crystals
liquid crystals
liquid
specific position
specific orientation
specific position
random orientation
random position
specific orientation
random position
random orientation
First semiconductor diodes
Very soft and difficult
Far IR detectors
Soft and difficult
Light Emitting Diodes, Lasers, Detectors
expensive
SiGe: stressors
SiC: radiation
Si: Transistors - $260billion industry
Columns II-VI build a “Lego-like” tool box for semiconductor Devices
Chemical differences lead to different bandgaps
Physical lattice mismatch leads to strain
  Can be design feature or a physical instability
Not all combinations possible:
  lattice mismatch, room temperature instability
Compound
IV-IV: Si-Ge, Si-C
Elemental (e.g., Si, Ge, C)
III-V: InP, GaAs, (InxGa 1-x)(AsyP 1-y)
IV-VI: PbS
II-VI: Hg1-xCdxTe
2)
1)
3)
4)
5)
6)

## Slide 30: Spatial Atomic Arrangements Position and Bond Orientation
solid crystals
plastic crystals
liquid crystals
liquid
specific position
specific orientation
specific position
random orientation
random position
specific orientation
random position
random orientation
Course will focus on solid materials with stable bonds:
“Solid State”
Cross section of a MOSFET
Crystalline

## Slide 31: Solid State Atomic Arrangements in MOSFETS
Cross section of a MOSFET
Substrate is a perfectly
arranged Si crystal
solid crystals
specific position
specific orientation
Crystalline
Poly-Crystalline
Amorphous
Oxides

## Slide 32: Functional Layers in MOSFETS
Cross section of a MOSFET
Device is a perfectly
arranged crystal
solid crystals
specific position
specific orientation
Crystalline
Poly-Crystalline
Amorphous
Oxides
Highly conductive
Electron transport
Conductive
Electron transport
Hold charge
Non-Conductive
“NO” transport
Dielectric
Semiconductor
Conductor
Poly-Si / metal
Gate
Device
Substrate is a perfectly
arranged Si crystal

## Slide 33: Functional Layers in MOSFETS
Cross section of a MOSFET
Device is a perfectly
arranged crystal
solid crystals
specific position
specific orientation
Crystalline
Poly-Crystalline
Amorphous
Oxides
Highly conductive
Electron transport
Conductive
Electron transport
Hold charge
Non-Conductive
“NO” transport
Dielectric
Semiconductor
Conductor
Poly-Si / metal
Gate
Device
Modern solid state devices use all forms these forms of materials
Focus on Crystals first – start with 1D => 2D => 3D
Transfer concepts of electronic behavior in crystals to other materials

## Slide 34: Section 2 Materials
2.1 Typical Semiconducting Materials
  Current flow in semiconductors (reminder)
  Elemental semiconductors in the periodic table
  Bonding for half-filled shells, column IV, III-V, and II-VI
2.2 Typical applications of elemental and compound semiconductors
2.3 Atomic Positions and Bond Orientations
  Solid State vs. other crystals
  Typical Atomic Arrangements in MOSFETS
Reference: Vol. 6, Ch. 1
34
One Video Segment
One Video Segment
One Video Segment

## Slide 36: Computing Carrier-Density and Velocity
Atomic composition
- number of electrons per atom
Arrangement of atoms
- not all electrons are available for conduction
For Periodic Arrays
- simplification for computation
• Concept of Unit Cells
• Simple 3-D Unit Cells