## Slide 1: Section 3 Crystals
Gerhard Klimeck
gekco@purdue.edu
Solid State Devices

## Slide 2: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment

## Slide 3: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment

## Slide 4: Crystals form the Core Device Material
Cross section of a MOSFET
Device is a perfectly
arranged crystal
solid crystals
specific position
specific orientation
Crystalline
Poly-Crystalline
Amorphous
Oxides
Highly conductive
Electron transport
Conductive
Electron transport
Hold charge
Non-Conductive
“NO” transport
Dielectric
Semiconductor
Conductor
Poly-Si / metal
Gate
Device
Modern solid state devices use all forms these forms of materials
Focus on Crystals first – start with 1D => 2D => 3D
Transfer concepts of electronic behavior in crystals to other materials

## Slide 5: One-dimensional Crystals
No realistic system is truly 1-D, but ….
1D properties dominate behavior in some material and devices
  Materials: e.g polymers,
  Biology: e.g. DNA
  Devices: e.g. 1D heterostructures (lasers, RTDs)
Can often be solved analytically, many properties have 2D/3D analogs
Polyacetylene
PPP
There is exactly ONE primitive unit cell in a 1D system

## Slide 6: Unit cells of a Periodic 2D Lattice
Unit cells are not unique
Unit cells can be Primitive or Non-primitive
“Infinitely” extended
2D shown
3D same concepts
NA=6 x 1023/mol
Can NEVER solve this, even on the largest computer
Simplify to a repeated (small) cell
b1
a1
b2
a2
b3
a3
b4
a4
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid

## Slide 7: Bravais Lattice
b1
a1
b2
a2
b3
a3
b4
a4
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid
every point has the same environment as every other point (same number of neighbors, next neighbors, …)

## Slide 8: Bravais Lattice with a Basis
b1
a1
b2
a2
b3
a3
b4
a4
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid
every point has the same environment as every other point (same number of neighbors, next neighbors, …)
Non-Bravais lattice
Bravais lattice
with a basis

## Slide 9: Graphene - Bravais Lattice with a Basis
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid
every point has the same environment as every other point (same number of neighbors, next neighbors, …)
Non-Bravais lattice
Bravais lattice
with a basis
A and B do not have
identical environments
A
B
This is a Graphene sheet which has “recently” been isolated from Graphite by adhesive tape stamping.
2005 - Novoselov, Geim, et al. Nature, 438, 197.
2010 – Nobel Prize in Physics
Conversion into a Bravais lattice:
Combine A and B into a single basis
Obtain a rhombic Bravais lattice
Original image from: http://en.wikipedia.org/wiki/File:Rhombic_Lattice.svg

## Slide 10: Bravais Lattice with a Basis
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid
every point has the same environment as every other point (same number of neighbors, next neighbors, …)
Non-Bravais lattice
Bravais lattice
with a basis
b1
a1
b2
a2
b3
a3
b4
a4
Unit cells are not unique
Unit cells can be Primitive or Non-primitive
Conversion into a Bravais lattice:
Combine complex components into a single repeated basis
Establish basis vectors

## Slide 11: Bravais Lattice with a Basis – in Art
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid
every point has the same environment as every other point (same number of neighbors, next neighbors, …)
Non-Bravais lattice
Bravais lattice
with a basis
b1
a1
b2
a2
b3
a3
b4
a4
Unit cells are not unique
Unit cells can be Primitive or Non-primitive
Escher Tiling
Kepler Tiling
Conversion into a Bravais lattice:
Combine complex components into a single repeated basis
Establish basis vectors

## Slide 12: Non-Periodic Repeated Cells NOT a Bravais Lattice
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid
every point has the same environment as every other point (same number of neighbors, next neighbors, …)
b1
a1
b2
a2
b3
a3
b4
a4
Unit cells are not unique
Unit cells can be Primitive or Non-primitive
Non-Bravais lattice
Bravais lattice
with a basis
Conversion into a Bravais lattice:
Combine complex components into a single repeated basis
Establish basis vectors
Ancient Tiles
Penrose Tiles
Two different unit cells in random order
… these CANNOT be transformed to Bravais lattice
ex. Aluminum-Manganese compounds, non-sticky coats
A Bravais Lattice must contain long-range order!

## Slide 13: How to define ONE primitive cell? Wigner-Seitz Primitive Cell
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid
every point has the same environment as every other point (same number of neighbors, next neighbors, …)
Non-Bravais lattice
Bravais lattice
with a basis
b1
a1
b2
a2
b3
a3
b4
a4
Unit cells are not unique
Unit cells can be Primitive or Non-primitive
Conversion into a Bravais lattice:
Combine A and B int a single basis
Obtain a rhombic Bravais lattice

## Slide 14: How to define ONE primitive cell? Wigner-Seitz Primitive Cell
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid
every point has the same environment as every other point (same number of neighbors, next neighbors, …)
b1
a1
b2
a2
b3
a3
b4
a4
Unit cells are not unique
Unit cells can be Primitive or Non-primitive
Eg.: oblique

## Slide 15: How to define ONE primitive cell? Wigner-Seitz Primitive Cell
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid
every point has the same environment as every other point (same number of neighbors, next neighbors, …)
Non-Bravais lattice
Bravais lattice
with a basis
Conversion into a Bravais lattice:
Combine A and B int a single basis
Obtain a rhombic Bravais lattice
Unit cells are not unique
Unit cells can be Primitive or Non-primitive
Choose a reference atom
Connect to all its neighbors
by straight lines
Draw lines (in 2D) or planes
(in 3D) normal to and at the
midpoints of connecting lines
Smallest area/volume enclosed
is the Wigner-Seitz primitive cell
Wigner-Seitz cell is ONE definition of a Unit Cell that always works
There are other ways of construction!
Need work on cell

## Slide 16: How to define ONE primitive cell? Wigner-Seitz Primitive Cell
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid
every point has the same environment as every other point (same number of neighbors, next neighbors, …)
Non-Bravais lattice
Bravais lattice
with a basis
Conversion into a Bravais lattice:
Combine A and B int a single basis
Obtain a rhombic Bravais lattice
Unit cells are not unique
Unit cells can be Primitive or Non-primitive
Choose a reference atom
Connect to all its neighbors
by straight lines
Draw lines (in 2D) or planes
(in 3D) normal to and at the
midpoints of connecting lines
Smallest area/volume enclosed
is the Wigner-Seitz primitive cell
Wigner-Seitz cell is ONE definition of a Unit Cell that always works
There are other ways of construction!

## Slide 17: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 18: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 19: Section 3 – Crystals 3.2 Tables of Bravais Lattices
Gerhard Klimeck
gekco@purdue.edu
Solid State Devices

## Slide 20: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 21: Bravais Lattices in 2D (5-types)
Original image from: http://upload.wikimedia.org/wikipedia/commons/e/ee/2d-bravais.svg
square
rectangular
hexagonal
Centered rectangular
or rhombic or triangular
2 atoms per unit cell!
Parallelogrammic or
oblique
Notes: corrections

## Slide 22: Bravais Lattices in 2D (5-types)
Original image from: http://upload.wikimedia.org/wikipedia/commons/e/ee/2d-bravais.svg
square
rectangular
hexagonal
Centered rectangular
or rhombic or triangular
2 atoms per unit cell!
Parallelogrammic or
oblique
Can construct all periodic 2D lattices from these basis sets
Notes: corrections

## Slide 23: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 24: Bravais lattice in 3D (14-types)
 | Triclinic | Cubic | Tetragonal | Orthorobmic | Rhombohedral | Hexagonal | Monoclinic
P |  |  |  |  |  |  | 
I |  |  |  |  |  |  | 
F |  |  |  |  |  |  | 
C |  |  |  |  |  |  | 
Rotation
points
primitve
Body centered
Face centered
Single face centered

## Slide 25: Bravais lattice in 3D (14-types)
 | Triclinic | Cubic | Tetragonal | Orthorobmic | Rhombohedral | Hexagonal | Monoclinic
P |  |  |  |  |  |  | 
I |  |  |  |  |  |  | 
F |  |  |  |  |  |  | 
C |  |  |  |  |  |  | 
Rotation
points
primitve
Body centered
Face centered
Single face centered
A
C

## Slide 26: Duplicated Bravais Lattice
Tetragonal FC = Tetragonal BC
c
A
c
A
A
C
Unlucky Frankenheim (1842)
counted 15 unit cells!
Bravais pointed out that 2 cells were duplicated
Tetragonal face centered
Tetragonal body centered
c

## Slide 27: Bravais lattice in 3D (14-types)
A
C

## Slide 28: 3 Dominant Bravais Lattices in Nature
Cubic conceptionally simple,
but experimentally very unusual
Polonium84
70-75% of all natural
crystalline materials

## Slide 29: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 30: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 31: Section 3 – Crystals 3.3 Density Definitions and Applications to Common Materials
Gerhard Klimeck
gekco@purdue.edu
Solid State Devices

## Slide 32: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 33: Simple Cubic Cubic Lattice: Number of atoms
Points per cell
=1/8 points/corner x 8 corners
=1 Point/cell
(depends on definition of cell)
Number density
= (1/a3) points/cm3
(does not depend on cell definition)
a

## Slide 34: Simple Cubic Cubic Lattice: Packing Density
Packing density
=volume filled/total volume
R=a/2 maximum radius
V=(4/3)pR3 Volume of a sphere
P= (1/8)x(4/3)pR3 x (8 corners) /a3
=p/6
~52%
(about HALF of the volume is EMPTY)
Typical for crystals and amorphous materials
(does not depend on cell definition)
a
a
R

## Slide 35: Simple Cubic Cubic Lattice: Areal Density
Areal density (face diagonal)
= (1/4 points/corner) x (4 corners)/2a2 cm-2
~0.7/a2 cm-2
Areal Density
=(1/4 per corner) x (4 corners)/a2
=1/a2 cm-2
Surfaces are critical in semiconductors:
Vertical stacking of materials => misalignment => dangling bonds => loose electrons
=> Different surface chemistry
Notes: Typo on the exponent (-3)

## Slide 36: Points per Cell Examples
BCC Points per cell
= 1/8 x 8 @corners
+ 1 @inside
=2
FCC Points per cell
= 1/8 x 8 @corners
+ 1/2 x 6 @faces
=4

## Slide 37: Hexagonal Closed-Packed
1/2 x 2 @faces =1
1/2x1/3 x 12 @corners =2
Points per cell
3 points/cell
top/bottom
neigbors

## Slide 38: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 39: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 40: Bravais Lattice with a Basis
Address every point in the lattice by integer translation of unit vectors
Property of ONE CELL defines the property of the solid
every point has the same environment as every other point (same number of neighbors, next neighbors, …)
Non-Bravais lattice
Bravais lattice
with a basis
b1
a1
b2
a2
b3
a3
b4
a4
Unit cells are not unique
Unit cells can be Primitive or Non-primitive
Conversion into a Bravais lattice:
Combine complex components into a single repeated basis
Establish basis vectors
Graphene
Bravais lattice
with a basis
NaCl
Rocksalt

## Slide 41: Rock-Salt as FCC lattice
=
For more discussion, see Kittel and Ashcroft/Mermin
NaCl is normal household cooking salt
We see the crystals every day – what is the crystal structure?
At first glance it looks like a simple cubic cell
one atom on each corner
But they are different => not a Bravais lattice
a basis of 2 atoms
arranged in FCC

## Slide 42: Zinc-Blende Lattice for GaAs
Atoms/cell=(1/8)x8 + (1/2)x6 + 4=8
Tetrahedral structure
Need work on animation

## Slide 43: GaAs Crystal Plotted in Crystal Viewer

## Slide 44: GaAs Crystal Without Bonds

## Slide 45: GaAs Crystal Just One Species

## Slide 46: GaAs Crystal Just One Species Focus on Few

## Slide 47: GaAs Crystal Just One Species Focus on Few – Take out a Few

## Slide 48: GaAs Crystal Just One Species A FCC Cell!
FCC cell – Atoms/cell = (1/8)x8 + (1/2)x6 = 4

## Slide 49: GaAs Crystal Just One Species A FCC Cell!
FCC cell – 4 atoms per unit cell

## Slide 50: GaAs Crystal Both Species
FCC cell – 4 atoms per unit cell – brown species

## Slide 51: GaAs Crystal Both Species
FCC cell – 4 atoms per unit cell – brown species
Focus on a few of the “blue species”

## Slide 52: GaAs Crystal Both Species
FCC cell – 4 atoms per unit cell – brown species
FCC cell – 4 atoms per unit cell – purple species

## Slide 53: GaAs Crystal Both Species
FCC cell – 4 atoms per unit cell – brown species
FCC cell – 4 atoms per unit cell – purple species

## Slide 54: GaAs Crystal Both Species
FCC cell – 4 atoms per unit cell – brown species
FCC cell – 4 atoms per unit cell – purple species

## Slide 55: GaAs Crystal – 2 FCC
Zincblende – 2 FCC bases – separated by [¼ ¼ ¼]

## Slide 56: Diamond FCC Lattice for GaAs and Silicon
Zincblende – GaAs - 2 FCC bases – separated by [¼ ¼ ¼]
Diamond – Si - 2 FCC bases – separated by [¼ ¼ ¼]

## Slide 57: Hexagonal Closed-Packed for CdS
(Cd) atoms/cell=
(1/6)x12 + (1/2)x2 + 3=6
Focus on (Cd) …

## Slide 58: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 59: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 60: Section 3 – Crystals 3.4 Surfaces, Miller Index
Gerhard Klimeck
gekco@purdue.edu
Solid State Devices

## Slide 61: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment
status

## Slide 62: Surface Reconstruction

## Slide 63: Miller-Indices and Definition of Planes

## Slide 64: Miller Indices: Simple Construction Process
Set up axes along the edges of unit cell
Normalize intercepts …. 2, 3, 1
Invert/rationalize intercepts … 1/2, 1/3, 1
3/6, 2/6, 6/6
4. Enclose the numbers in curvilinear brackets
(326)
x
y
z

## Slide 65: Miller Indices: Additional Cases
x
y
z
x
y
z
2, 3, -2
1/2, 1/3, -1/2
3, 2, -3
_
(3 2 3)
2, 3, 
1/2, 1/3, 0
3, 2, 0
(3 2 0)
Negative Intercept
Intercept at infinity

## Slide 66: Miller Indices and Vector Algebra
x,a
y,b
z,c
Miller indices: (326)
Normal to the surface and R1,R2
R2xR1= = 3a + 2b + 6c
Vector indices same as Miller indices !
(326) vs. [326]
R1= 1c – 2a
R2 = 3b – 2a
Specification of vectors normal to a particular plane!

## Slide 67: Angle between Two Planes
x
y
z
x
y
z
Angle between two vectors
Dot product / inner product between two vectors
Typo on equation

## Slide 68: Examples …
x
y
z
cos(q)=(1x0+0x1+0x1)/(1x2) = 0
so q=90 degrees
(011) surface is normal to (100) surface

## Slide 69: Examples … Ingot rotated in the coordinate system
cos(q)=(1x0+0x1+0x1)/(1x2) = 0
so q=90 degrees
(011) surface is normal to (100) surface

## Slide 70: Example: Find the [021] direction
N1•T =cos(q1)=(1x0+0x2+0x1)/(1x5) = 0, so q=90 degrees
[021] vector lies on (100) plane.
[021]
N2•T =cos(q2)=(0x0+2x1+1x1)/(5 2) = 3/ 10, so q=18.43 degrees
with respect to [011] direction.
[011]
[100]
q1
q2
[021]
[011]
Notes: Typo on formula on the bottom

## Slide 71: Bravais-Miller Indices
a1
z
a2
a3
, 1, -1, 
0, 1, -1, 0
0, 1, -1, 0
(0 1 1 0)
First three indices sum to zero.

## Slide 72: Crystals form the Core Device Material
Cross section of a MOSFET
Device is a perfectly
arranged crystal
solid crystals
specific position
specific orientation
Crystalline
Poly-Crystalline
Amorphous
Oxides
Highly conductive
Electron transport
Conductive
Electron transport
Hold charge
Non-Conductive
“NO” transport
Dielectric
Semiconductor
Conductor
Poly-Si / metal
Gate
Device
Modern solid state devices use all forms these forms of materials
Focus on Crystals first – start with 1D => 2D => 3D
Transfer concepts of electronic behavior in crystals to other materials

## Slide 73: Summary
Crystalline material can be built by repeating the basic building blocks. This simplifies the quantum solution of the material, which will allow us to compute n and v for these systems easily.
Silicon, GaAs, PbS do not have simple Bravais lattice; but they have Bravais lattice with a basis.
Often we need to calculate the direction of crystal planes because material properties differ along different planes. Miller indices are one useful way of characterizing crystal planes. It is useful to review some identities of vector calculus to such calculations involving crystal planes.

## Slide 74: Section 3 Crystals
3.1 Crystal definitions
  One-dimensional Crystals – simple primitive cell
  Unit cells of a Periodic 2D Lattice
  Bravais lattice
  Bravais lattice with a basis
  Non-periodic repeated cells
  Definition of ONE Primitive Cell – Wigner-Seitz Cell
3.2 Tables of Bravais Lattices
  Bravais Lattices in 2D (5 types)
  Bravais Lattices in 3D (14 types)
  3 Dominant Bravais Lattices in Nature
3.3 Density Definitions and Applications to Common Materials
  Number, Packing, and Areal Density
  Common Crystals – Non-Primitive Unit Cells (NaCl, GaAs, CdS)
3.4 Surfaces, Miller Index
Reference: Vol. 6, Ch. 1, ABACUS tool at nanohub.org/tools/abacus and
"Crystal Viewer Lab, https://nanohub.org/resources/crystalviewer
One Video Segment
One Video Segment
One Video Segment
One Video Segment