## Slide 1: Section 19 Introduction to PN Junctions
Solid State Devices

## Slide 2: Current Flow Through Semiconductors
Transport with scattering, non-equil. Stat. Mech.
Drift-diffusion Eq. with recombination-generation
Understanding transport in concrete devices
Materials, composition, crystals
Tabulated for “known” bulk materials
At nm-scale properties change with geometry => theory
Equilibrium Statistical Mechanics
Occupation factors
Quantum Mechanics Mechanics
Concepts of density of states and masses
PN Diode
Schottky Diode
BJT/ HBT
MOS

## Slide 3: Topic Map
 | Equilibrium |  |  |  | 
PN Diode
Schottky Diode
BJT/ HBT
MOS

## Slide 4: Topic Map
 | Equilibrium | DC |  |  | 
PN Diode
Schottky Diode
BJT/ HBT
MOS

## Slide 5: Topic Map
 | Equilibrium | DC | Small signal | Large Signal | Circuits
PN Diode
Schottky Diode
BJT/ HBT
MOS

## Slide 6: Section 19 Introduction to PN Junctions
 | Equilibrium | DC | Small signal | Large Signal | Circuits
PN Diode
Schottky Diode
BJT/ HBT
MOS
Diode in Equilibrium.
(No external voltage applied)

## Slide 7: Section 19 Introduction to PN Junctions
19.1 Structure and Depletion Region
19.2 Drawing band-diagrams in equilibrium
Vid
Vid

## Slide 8: What is a Diode good for ….
solar cells
GaAs lasers
GaN lasers
Avalanche Photodiode
Organic LED
Notes: 28 slides … do not waste time …

## Slide 9: p-n Junction Devices …
Schematic of a p-n Diode
Contact
Contact
P-doped pocket
N-doped
substrate
N
P
Symbol
Point-contact diode
https://upload.wikimedia.org/wikipedia/commons/8/8c/CatWhisker.jpg

## Slide 10: P and N doped Material Side by Side …
N-doped
Conduction Band
Valence Band
Ec
EV
EF
k
-k
E
P-doped
Conduction Band
Valence Band
EF
For P-doped
EF close to EV
Vacuum level (determined by material)

## Slide 11: Forming a Junction
Space charge (fixed)
Mobile carriers
Donor-side (N-side)
Squares are fixed donor atoms.
Every donor atom has given away one electron (blue circle)
Acceptor-side (P-side)
Squares are fixed acceptor atoms.
Every acceptor atom has captured one electron (from the valence band).
Every acceptor atom leaves behind one hole in the valence band. (red circle)
Notes: Nd-side: Squares are donor atoms fixed in space. The donor atoms have each given away one electron (blue circle). Every green square is matched with a blue circle.
Na-side: Squares are acceptor atoms. Each acceptor atom captures one electron from the valence band. This leaves behind a positive hole (red circle).

## Slide 12: Forming a Junction
Space charge (fixed)
Mobile carriers
Junction
x
Before joining the p and the n side
Valid only in equilibrium
Notes: Nd-side: Squares are donor atoms fixed in space. The donor atoms have each given away one electron (blue circle). Every green square is matched with a blue circle.
Na-side: Squares are acceptor atoms. Each acceptor atom captures one electron from the valence band. This leaves behind a positive hole (red circle).

## Slide 13: Forming a Junction
Junction
Actual Carrier Concentrations
Bulk Region
Bulk Region
Depleted
Region
n-side
p-side
n
n
p
p
ln(n),
ln(p)
x
x
Space charge (fixed)
Mobile carriers
Before joining the p and the n side
After joining the p and the n side
Depletion approximation
Depletion approximation
Diffusion
E-field

## Slide 14: Formation of a Junction
+
ln(ND)
ln(n)
Q=p-n+ND-NA
Bulk Region
qND
-qNA
Bulk Region
xn
Depleted Region
xp
ln(NA)
ln(p)
Net charge on N-side: qND
(subtract green from blue line)
Space charge region: fixed donor atoms
Neglect electrons in p-side
Xn: depletion region in N-side
Net charge on P-side: -qNA
(subtract brown from red line)
Space charge region: fixed acceptor atoms
Xp: depletion region in P-side
red and blue are of equal size  charge balance
Depletion Region means depleted of “mobile” charges
Notes: Figure 3) Net charge is qNd on N-side depletion region. (Subtract green from blue line) qNd is a fixed space charge. Similar argument for P-side.
Blue and red area have to be the same; Charge balance.

## Slide 15: Potential, Field and Charge
In most practical cases start from charge and derive potentials!
=> Useful to learn “graphical” integration
From Section 13 – Band Diagrams

## Slide 16
In most practical cases start from charge and derive potentials!
=> Useful to learn “graphical” integration
Potential, Field and Charge
From Section 13 – Band Diagrams

## Slide 17: Sketch of Electrostatics
position
Potential
position
E-field
p-n+ND-NA
qND
Depleted
Region
position
Bulk Region
-qNA
Bulk Region
xp
Vbi
xn
Integrate
Integrate

## Slide 18: Sketch of Electrostatics
position
Potential
position
Band Diagram
xn
xp
Invert to go from potential to energy scale
In equilibrium Fermi-level must be flat

## Slide 19: Section 19 Introduction to PN Junctions
19.1 Structure and Depletion Region
19.2 Drawing band-diagrams in equilibrium
Vi
Vid
status

## Slide 20: Section 19 Introduction to PN Junctions
19.1 Structure and Depletion Region
19.2 Drawing band-diagrams in equilibrium
Vi
Vid
status

## Slide 21: Section 19 Introduction to PN Junctions
Solid State Devices
19.2 Drawing band-diagrams in equilibrium

## Slide 22: Section 19 Introduction to PN Junctions
19.1 Structure and Depletion Region
19.2 Drawing band-diagrams in equilibrium
Vid
Vid
status

## Slide 23: Drawing Band Diagram in Equilibrium…
Equilibrium
(Start here)
Non-Equilibrium (refine later)
DC dn/dt=0
Small signal dn/dt ~ jwt x n
Transient --- full solution
Previously constant in homogeneous semiconductors. But for pn diode: f(x) !!
In equilibrium J=0 (no current flow).
But, Electric fields or diffusion might still be present.  Detailed balance

## Slide 24: Short-cut to Band-diagram
… is equivalent to solving the Poisson equation
Vacuum level
EC
EV
EF
c2
c1
Neutral
Neutral
Space Charge
Drawing Recipe
Start with EF
Ec/Ev in bulk n-side
Ec/Ev in bulk p-side
Vacuum level in N
Vacuum level in P
Join vacuum levels
“Transfer” vacuum slopes to join Ec/Ev

## Slide 25: Built-in Potential: boundary conditions @infinity
qVbi
D1
D2
c1
c2
Eg,2
Always true in equilibrium
Built-in potential Vbi unknown!
D1,2 determined via doping concentrations
X1,2 material parameters

## Slide 26: Interface Boundary Conditions
position
E = (D/kεo)
xn
xp
position
D
xn
xp
Displacement is continuous across the interface, field need not be ..
Homo - Junction
Hetero - Junction
Field not continuous across junction

## Slide 27: Built-in voltage for Homo-junctions
Neutral
Neutral
Space Charge
Vacuum level
EC
EV
EF
c1
c1
qVbi
Drawing Recipe
Start with EF
Ec/Ev in bulk n-side
Ec/Ev in bulk p-side
Vacuum level in N
Vacuum level in P
Join vacuum levels
“Transfer” vacuum slopes to join Ec/Ev
Zero for homo-junctions

## Slide 28: Analytical Solution of Poisson Equation
Q= p-n+ND-NA
qND
Depleted Region
position
-qNA
xn
xp

## Slide 29: Analytical Solution for Homojunctions
(Charge)
p-n+ND-NA
qND
-qNA
xn
xp
position
E-field
position
position
Potential
Vbi
Small !
Integrate
Integrate
E-field
Potential
Integrate

## Slide 30: Depletion Regions in Homojunctions
xn
xp
Small Project: Solve the same problem for a hetero-junction
Neutral
Neutral
Space Charge
Solve for xn, xp

## Slide 31: Complete Analytical Solution
N
P
-xp
0
xn
x
qND
-qNA
ρ
xn
-xp
E
-xp
xn
0
x
x
x
V
-xp
xn
Integrate
Integrate
If you need to calculate electric field at specific points…

## Slide 32: Summary PN-Junction Electrostatics
Learning to draw band-diagrams is one of the most important topics you learn in this course. Band-diagrams are a graphical way of quickly solving the Poisson equation.
If you consistently follow the rules of drawing band-diagrams, you will always get correct results. Try to follow the rules, not guess the final result.
Drawing Recipe
Start with EF
Ec/Ev in bulk n-side
Ec/Ev in bulk p-side
Vacuum level in N
Vacuum level in P
Join vacuum levels
“Transfer” vacuum slopes to join Ec/Ev

## Slide 33: Section 19 Introduction to PN Junctions
19.1 Structure and Depletion Region
19.2 Drawing band-diagrams in equilibrium
Vid
Vid
Drawing Recipe
Start with EF
Ec/Ev in bulk n-side
Ec/Ev in bulk p-side
Vacuum level in N
Vacuum level in P
Join vacuum levels
“Transfer” vacuum slopes to join Ec/Ev
Learning to draw band-diagrams is one of the most important topics you learn in this course. Band-diagrams are a graphical way of quickly solving the Poisson equation.
If you consistently follow the rules of drawing band-diagrams, you will always get correct results. Try to follow the rules, not guess the final result.