## Slide 1: Section 20 PN Diode I-V Characteristics
Solid State Devices

## Slide 2: Section 20 PN Diode I-V Characteristics
 | Equilibrium | DC | Small signal | Large Signal | Circuits
PN Diode
Schottky Diode
BJT/ HBT
MOS
Diode in DC Bias

## Slide 3: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Tunneling
  Impact ionization
status
V
V
V
V

## Slide 4: Forward and Reverse Bias
Forward Bias
Reverse Bias
Current flows easily
Current does not flow easily

## Slide 5: Applying Bias to p-n Junction
VA
2
4
5
1
3
6,7
ln(I)
Diffusion limited
Ambipolar transport
High injection
R-G in depletion
Breakdown
Trap-assisted R-G
Esaki Tunneling
Forward Bias
Reverse Bias
IV characteristics of a Diode
To be discussed in detail

## Slide 6: Band Diagram with Applied Bias…
Next segment / lecture …
Band diagram (this segment)

## Slide 7: Applying a Bias: Poisson Equation
EF-EV
EC-EF
qVbi
EC-Fn
q(Vbi-V)
Fp-EV
-qV
Question: Max value of Vbi?
No bias
Applied bias
P-side grounded
Answer: for degenerate s.c.,
if EC-EF=0, EF-EV=0  Eg
Notes: Ec-Fn must remain the same. Fp-Ev must remain the same (Even under bias). Quasi-Fermilevel: Fermilevel in the presence of a bias.
Beta is 1/kt. In equilbrium Fn=Fp.

## Slide 8: Depletion Widths
xn
xp
GND
-V
From previous lecture (homo-junction)
Applied bias

## Slide 9: Depletion Widths
xn
xp
GND
-V
From previous lecture (homo-junction)
Applied bias
N
P

## Slide 10: Fields and Depletion at Forward/Reverse Biases
Charge
Electric Field
Potential
Position
Position
Position
VA=0
VA=0
VA=0
VA=0
VA=0
N
P
Zero Bias

## Slide 11: Fields and Depletion at Forward/Reverse Biases
Charge
Electric Field
Potential
Position
Position
Position
VA>0
VA>0
VA>0
VA=0
VA=0
N
P
VA>0
VA>0
Forward Bias

## Slide 12: Fields and Depletion at Forward/Reverse Biases
Charge
Electric Field
Potential
Position
Position
Position
VA<0
VA=0
VA=0
N
P
VA>0
VA>0
VA<0
VA<0
Reverse Bias

## Slide 13: Fields and Depletion at Forward/Reverse Biases
Charge
Electric Field
Potential
Position
Position
Position
VA<0
VA=0
N
P
VA>0
VA<0
VA<0
Reverse Bias

## Slide 14: Fields and Depletion at Forward/Reverse Biases
Charge
Electric Field
Potential
Position
Position
Position
VA=0
VA=0
VA>0
VA=0
VA=0
N
P
Zero Bias
VA=0
VA>0
VA<0

## Slide 15: Fields and Depletion at Forward/Reverse Biases
Charge
Electric Field
Potential
Position
Position
Position
VA>0
N
P
VA>0
Forward Bias
VA=0
VA>0
VA<0

## Slide 16: Fields and Depletion at Forward/Reverse Biases
Charge
Electric Field
Potential
Position
Position
Position
VA=0
VA=0
VA>0
VA=0
VA=0
N
P
Zero Bias
VA=0
VA>0
VA<0
Barrier height is reduced at forward biases
Significant increase of peak field at reverse
bias

## Slide 17: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Tunneling
  Impact ionization
status
V
V
V
V

## Slide 18: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Impact ionization
  Tunneling
status
V
V
V
V

## Slide 19: Section 20 PN Diode I-V Characteristics
Solid State Devices
20.2 Derivation of the forward bias formula

## Slide 20: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Impact ionization
  Tunneling
status
V
V
V
V

## Slide 21: Various Regions of I-V Characteristics
Diffusion limited
Ambipolar transport
High injection
R-G in depletion
Breakdown
Trap-assisted R-G
Esaki Tunneling
VA
2
4
5
1
3
6,7
ln(I)
1
1. Diffusion limited
Notes: Asad: We should redraw the figure ….

## Slide 22: Recall: One Sided Minority Diffusion
Steady state
Acceptor doped
Fp-EV
q(Vbi-V)
-V
If current is continuous, one can calculate
for the current anywhere. Position doesn’t
matter! Calculate at “easiest” position.
Minority carrier current on p-side.
We know the solution from earlier
Assume steady state, no rn, gn

## Slide 23: Boundary Conditions
Fp
Fn
q(Vbi-VA)
-VA
Boundary Conditions
Solution profile
Difference of Quasi-Fermi-levels equals applied voltage
X=0+

## Slide 24: Right Boundary Condition
Infinite surface recombination velocity at metal  excess carrier concentration = 0
Fp
Fn
q(Vbi-VA)
-VA
Solution profile
X=0+

## Slide 25: Example: One Sided Minority Diffusion
Ansatz
Final result: Excess electron carrier concentration (P-side) as function of position
Plug in B.C.
Fp
Fn
q(Vbi-VA)
-VA
Solution profile
X=0+

## Slide 26: Electron & Hole Fluxes
Fp
Fn
Dn
Dp
Current (electrons)
Current (holes)

## Slide 27: Total Current
But we have only expressions at different x-points
Diffusion current
Fp
Fn
Dn
Dp
Current (electrons)
Current (holes)
To get total current, add electron and hole current values at identical x-points.
If there is no R-G in junction, => then the diffusion currents will be continuous
=> Add the 2 components

## Slide 28: Ideal pn-junction current
1
1
Diffusion current
Slope = 1

## Slide 29: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Impact ionization
  Tunneling
status
V
V
V
V

## Slide 30: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Impact ionization
  Tunneling
status
V
V
V
V
status
status

## Slide 31: Section 20 PN Diode I-V Characteristics
Solid State Devices
20.2 Forward Bias - Non-linear Regime

## Slide 32: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Impact ionization
  Tunneling
status
V
V
V
V
status
status

## Slide 33: Nonlinear Regime (3) …
VA
2
1
3
6,7
ln(I)
Assumption of flat Quasi-Fermi levels invalid here
Nonlinear Regime (2,3)

## Slide 34: Flat Quasi-Fermi Level up to Junction ?
Fp
Fn
Wn
Rewrite n into non-equilibrium form
New diffusion component: Plug this into original Jn equation
Drop of Quasi-Fermi level across the junction proportional to current!
Ignore variation in temperature in x
resistivity

## Slide 35: Forward Bias: Nonlinear Regime …
DFp
Dn
DFn
Still diffusion dominated transport? Since Quasi-Fermi levels are not flat in nonlinear regime (drift), this approximation becomes worse.
VA

## Slide 36: Current and Fermi Level Drop – A general concept
n can be derived from a complex quantum DOS
Opportunity to link Classical and Quantum Transport
Journal of Computational Electronics 2: 177–182, 2003

## Slide 37: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Impact ionization
  Tunneling
status
V
V
V
V
status

## Slide 38: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Impact ionization
  Tunneling
status
V
V
V
V
status

## Slide 39: Region (2): Ambipolar Transport
VA
2
1
3
6,7
ln(I)
Ambipolar Transport regime (2)
Question: Where does the 2 come from?

## Slide 40: Nonlinear Regime: Ambipolar Transport
Note: junction never disappears, even for large forward bias!
Electric field is not really negligible, but we do it anyhow….
Here not negligibly small. Ambipolar transport !
Excess carrier concentrations Thus…
Currents
Previously considered: p-side:
Ambipolar: minority AND majority carrier distribution is modified!

## Slide 41: Region (2): Ambipolar Transport
VA
2
1
3
6,7
ln(I)
Ambipolar Transport regime (2)

## Slide 42: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Tunneling
  Impact ionization
status
Video
V
V
V
status
status

## Slide 43: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Tunneling
  Impact ionization
status
Video
V
V
V

## Slide 44: Section 20 PN Diode I-V Characteristics
Solid State Devices
20.3 Non-Ideal Effects

## Slide 45: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Tunneling
  Impact ionization
status
V
V
V
V

## Slide 46: (4,6) Junction Recombination
Mass action in non-equilibrium

## Slide 47: (4,6) Junction Recombination
Assume
What is the recombination current?
Shockley-Reed Hall
Follows from assuming midgap traps

## Slide 48: Electron/Hole Concentrations at Junction
position

## Slide 49: Junction Recombination

## Slide 50: Junction Recombination in Forward Bias
VA
2
4
5
1
3
6,7
ln(I)
Emax
Effective spatial width of recombination
Excess Carrier at mid-junction
Factor ½ indicates recombination / traps in junction
Traps hidden in t
Keep positive branch
Approximate electric field as constant

## Slide 51: Junction Leakage in Practice
n
p
d
rj
rj
Insulating Layer
Junction Design Considerations
Electric field stronger at corners, sharp edges.  increased recombination!

## Slide 52: Junction Recombination in Reverse Bias
W=xn+xp
(Recombination in
depletion region
n=p=0)
Depletion width
Assume
Shockley-Reed Hall
Follows from assuming midgap traps

## Slide 53: Junction Recombination in Reverse Bias
VA
2
4
5
1
3
6,7
ln(I)
W=xn+xp
(Recombination in
depletion region
n=p=0)
Integrate…
Depletion width
Ideally the flat – now it depends as a square root of voltage => another probe mechanism for traps in junction

## Slide 54: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Tunneling
  Impact ionization
status
V
V
V
V

## Slide 55: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Tunneling
  Impact ionization
status
V
V
V
V

## Slide 56: Forward Bias Nonlinearity (7): Esaki Diode
I
VA
Fn
Fp
Fn
Fn
Fp
Fp
X
VA
2
1
3
6,7
ln(I)
Heavy doping
1
empty
No states!
Esaki-Diode: Heavily doped diode
Tunneling in diodes.
Nobel Prize (Esaki)

## Slide 57: Reverse Bias (5): Zener Tunneling
Fn
Fp
4
5
+VA
empty
empty
Tunneling
(triangular barrier)
Remember: Tunneling through a triangular barrier
Zener tunneling occurs in every diode. (reverse bias)

## Slide 58: Various Regions of I-V Characteristics
Diffusion limited
Ambipolar transport
High injection
R-G in depletion
Breakdown
Trap-assisted R-G
Esaki Tunneling
VA
2
4
5
1
3
6,7
ln(I)
Notes: Asad: We should redraw the figure ….

## Slide 59: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Tunneling
  Impact ionization
status
V
V
V
V

## Slide 60: Avalanche Breakdown
Diffusion limited
Ambipolar transport
High injection
R-G in depletion
Breakdown
Trap-assisted R-G
Esaki Tunneling
VA
2
4
5
1
3
6,7
ln(I)
Notes: Asad: We should redraw the figure ….

## Slide 61: Nonlinearity due to Impact-Ionization
Reverse Bias

## Slide 62: Nonlinearity due to Impact-Ionization
Reverse Bias

## Slide 63: Nonlinearity due to Impact-Ionization
Exponential current growth
(Impact Ionization or Inverse Auger process)
High Reverse Bias > bandgap (typically 3/2 bandgap)
Reverse Bias

## Slide 64: Nonlinearity due to Impact-Ionization
Exponential current growth
(Impact Ionization or Inverse Auger process)
High Reverse Bias > bandgap (typically 3/2 bandgap)
Reverse Bias

## Slide 65: Impact-ionization and Flux Conservation
x
W
0
Impact Ionization probabilities
Steady state: Define
IT = IN+IP (total current)
Constant in steady state
Differential equation

## Slide 66: Impact-ionization and Flux Conservation
Differential equation
x
W
0
Ip(W)~0
In(0)~0
Solution form of differential equation
Reverse diffusion current

## Slide 67: Impact-ionization
x
W
0
Ip(W)~0
In(0)~0
Solution form of differential equation
Reverse diffusion current
At x=W, IN has grown exponentially, and IP is now negligible.
Multiplication Factor

## Slide 68: Impact-ionization
x
W
0
Assume:
this cannot be quite right… n, p different masses etc
Electric Field
Position
VA<0
VA=0
VA>0
Assume:
Most avalanche happens spatially at maximum electric field
from experiment and theory A and B material coeffients
Breakdown-Field

## Slide 69: Impact-ionization: In Practice
Good ….
Imagers single photon can create an avalanche
Bad….
n
p
Insulating Layer
d
rj
rj
Photon Detector
High E-fields at junction corners  Breakdown

## Slide 70: Junction Engineering
E
E
Reduced field for p-i-n junction, because Vbi
(area under the curve) must be the same.
n
p
Insulating Layer
d
rj
rj
i-region
Lower E-field!
Intrinsic region: E-field has to be constant, because there are no charges!
High practical relevance for MOSFET scaling Needed to reduce fields on the drain side….

## Slide 71: Modern Considerations: Dead Space
For very small (ballistic) junctions, electrons can cross the junction without inducing impact Ionization.
(Dead space too small)
W
Dead Space
Dead Space:
Space you need before an electron can impact ionize.

## Slide 72: Zener Breakdown vs. Impact Ionization
How do you differentiate between
Zener tunneling and
impact-ionization?
Need bias > bandgap
Can happen for smaller reverse bias ~1V
Very noisy – can be measured

## Slide 73: Non-Ideal Effects: Conclusion
Junction recombination is often used as a diagnostic tool for process maturity. Defects in junction arises from misplaced donor impurities, not necessary from deep-trap impurities.
Impact ionization plays an important role in wide variety of devices (e.g. avalanche photo-diodes).

## Slide 74: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Tunneling
  Impact ionization
status
V
V
V
V

## Slide 75: Section 20 PN Diode I-V Characteristics
20.1 Band diagram with applied bias
20.2 Derivation of the forward bias formula
20.3 Forward Bias - Non-linear Regime
  Resistive drop
  Ambipolar regime
20.4 Non-ideal effects:
  Junction recombination
  Tunneling
  Impact ionization
V
V
V
V